## Slide 1: Performance Impact of Post-Regrowth Channel Etching on InGaAs MOSFETs Having MOCVD Source-Drain Regrowth
Device Research Conference 2013
Notre Dame, Indiana
6/24/2013
Andrew D. Carter1, S. Lee1, D.C. Elias1, C.-Y. Huang1, J. J. M. Law1, W. J. Mitchell1, B. J. Thibeault1, V. Chobpattana2, S. Stemmer2, A. C. Gossard1, and M. J. W. Rodwell1
1ECE Department, 2Materials Department,
University of California, Santa Barbara, CA 93106

## Slide 2: Overview
Why III-V for VLSI?
Device Physics and Scaling
Process Flows
Measurements
Conclusions

## Slide 3: Why III V VLSI?
Higher electron velocities than Si MOS
  For short Lg FETs,
  Transconductance,
  Jd and gm are key figures of merit in VLSI
However:
  Jd and gm degraded by source large Raccess
  Jd and gm degraded by interface trap density, Dit
Therefore, we must develop:
  Low access resistance source/drain contacts
  Thin, high-k, low Dit dielectrics on InGaAs
  Fully self-aligned process modules
MOSFETs have been, and always will be, a materials challenge.
1/Ron
Jd,max
gm

## Slide 4: FET Device Physics
Dit problem
  ↑Cit , ↓ Vsurface
  Vsurface supplies Cdos
  ↓ Vsurface =↓ ndos in Cdos
Electron band diagram: gate-insulator-channel

## Slide 5: Candidate III-V Planar Geometries
Intel IEDM 2009
“Trench” MOSFET
Leverages HEMT tech.
Gate oxide  Low Ig 
Small footprint 
But
Will the Lg scale?
Replacement Gate MOSFET
Easily defined Lg 
Gate oxide 
Small footprint 
But
Is RG doping high enough?
DRC 2013

## Slide 6: Gate Replacement FET Process Flow
6
MBE S/D Regrowth
Low-damage process Thermal gate metal No/Low-damage plasma Dielectric post-regrowth
STEM FET cross section, color-coded by chemistry Figure courtesy Jeremy Law (UCSB)
100 nm Lg
10 nm Thick Well
InAs
S/D
Nickel Gate Metal
InAlAs Back Barrier
DRC 2013

## Slide 7: Gate Replacement FET Challenges
MBE regrowth is non-selective  requires photoresist planarization
SEM of dummy gate
DRC 2013

## Slide 8: Gate Replacement FET Challenges
Short dummy gates are hard to planarize, aspect-ratio-limited gate length
Photoresist
Regrowth
DRC 2013

## Slide 9: Solution: MOCVD S/D Regrowth *
MBE is non-selective to the SiO2 pillar, while MOCVD is selective!
 PR planarization no longer necessary  short Lg that will not fall over
MBE InAs RG
MOCVD InGaAs RG
* Terao et al, APEX 2011, and Egard et al, DRC 2011
DRC 2013

## Slide 10: MBE Versus MOCVD S/D Regrowth
68 Lg, (1 nm Al2O3/ 4 nm HfO2), 10 nm channel, MOCVD InGaAs Regrowth
81 nm Lg, (1 nm Al2O3/ 4 nm HfO2), 10 nm channel, MBE InGaAs Regrowth
result
Similar on-state performance, but large Vth shift, poor SS, DIBL
DRC 2013

## Slide 11: Poor subthreshold: Channel Degradation
> 300 mV/dec subthreshold swing  Dit ? Channel degradation?
Experiment: SiO2 capping + high temp anneal + strip  MOSCAP 5 nm Al2O3
Large dispersion  Large Dit
InP channel capping for RG  large subthreshold swing for FETs 
DRC 2013

## Slide 12: MOCVD: Digital Channel Etching
Digital semiconductor etching*
Before ALD deposition: Oxidize channel surface (UV O3) Etch oxide in HCl:DI
Repeat as needed
Etches ~ 1.2 nm per cycle
* S.Lee et al, IPRM 2013
Top-down thin channels  Increase Cdepth
Simultaneous damage removal and body scaling
DRC 2013

## Slide 13: MOCVD RG with Digital Channel Etching
65 nm actual Lg, (1 nm Al2O3/ 4 nm HfO2) 2 cycles of digital etching (~ 6.5 nm channel)
68 nm actual Lg, (1 nm Al2O3/ 4 nm HfO2), No digital etching (~ 10 nm channel)
result
All devices improve with channel etch  thinner channel, remove surface damage

## Slide 14: MOCVD RG with Digital Channel Etching
result
All devices improve with channel etch  thinner channel, remove surface damage
 |  |  | gm map |  |  | 
1 | 1.10 | 0.90 |  |  |  | 
2 | 0.89 | 0.92 | 1.00 |  |  | 
3 | 0.93 | 0.90 | 1.10 |  |  | 
4 | 1.01 | Blank | 1.09 | 0.91 | 1.16 | 
5 | Open | 1.01 | 1.11 | 1.03 | 0.92 | 1.05
6 | 0.99 | 1.00 | 0.96 | Open | 0.88 | Open
 | A | B | C | D | E | F
 |  |  | gm map |  |  | 
1 | 1.38 | 1.50 |  |  |  | 
2 | 1.50 | 1.45 | 1.51 |  |  | 
3 | 1.50 | 1.21 | 1.53 | 1.53 |  | 
4 | 1.38 | Blank | 1.45 | 1.53 | 1.48 | 
5 | 1.15 | 1.58 | 1.42 | 1.36 | 1.26 | 1.47
6 | 1.09 | 1.38 | 1.42 | 1.47 | 1.39 | 1.50
 | A | B | C | D | E | F
Peak transconductance (mS/micron):
50 nm as drawn gate length, 0.5 V Vgs
No Etching (10 nm ch.)
2 Cycle Etching (~6.5 nm ch.)

## Slide 15: MOCVD RG with Digital Channel Etching
result
All devices improve with channel etch  thinner channel, remove surface damage

## Slide 16: MOCVD RG with Digital Channel Etching
result
Lower performance for not etched channels not due to metal-RG contact
DRC 2013

## Slide 17: MOCVD RG: Recent Results
48 nm gate length, ~ 3.8 nm HfO2, InGaAs with 2 cycle digital etching, p-doped back barrier
40 nm gate length, ~ 3.6 nm HfO2 , InAs/InGaAs channel, digitally etched *
* S. Lee et al, VLSI 2013
High performance III-V MOS using aggressively scaled ALD dielectrics

## Slide 18: Conclusions
65 nm gate last InGaAs MOSFET process flow using MOCVD
Jdrain = 0.78 mA/mm at 0.5 V Vgs – Vth , 0.5 V Vds
Peak transconductance: 1.58 mS/micron at 0.5 V Vds
Self-aligned process path for sub-50 nm III-V VLSI
Continued research areas
Thinner gate dielectrics
  Body scaling (thin planar QW and/or FinFETs)
  Improved Dit passivation techniques

## Slide 19: Thanks for your time! Questions? contact address: adc [at] ece.ucsb.edu
This research was supported by the SRC Non-classical CMOS Research Center (Task 1437.009). A portion of this work was done in the UCSB nanofabrication facility, part of NSF funded NNIN network and MRL Central Facilities supported by the MRSEC Program of the NSF under award No. MR05-20415.

## Slide 20: BACK UP SLIDES

## Slide 21: Source-Drain Regrowth Data

## Slide 22: MOCVD RG: Recent Results
48 nm gate length, ~ 3.8 nm HfO2, InGaAs with 2 cycle digital etching, p-doped back barrier
40 nm gate length, ~ 3.6 nm HfO2 , InAs/InGaAs channel, digitally etched *
* S. Lee et al, VLSI 2013
High performance III-V MOS using aggressively scaled ALD dielectrics

## Slide 23: FET Device Physics
*Ceffective includes Cox, Cdepth, Cdos
Electron band diagram of a quantum well FET

## Slide 24: FET Device Scaling
Si CMOS scaling: Contacted gate pitch 4x the gate length1)
4:1 reduction of contact area2)  4:1 reduction of rcontact
22 nm node  33 nm LS/D  For LS/D = LT, requires 5x10-9 ohm-cm2 rcontact
Contacted Gate Pitch
LS/D
Lg
WS/D
1) S. Natarajan, et al, IEDM 2008.
2) M.J.W. Rodwell, et al, IPRM 2010.
LS/D
Lg

## Slide 25: Gate First FET Process Flow
Thick (10 nm) channel
  Process damage mitigation
Heavy ( ~ 9x1012 cm-2) d doping
  Prevents ungated sidewall current choke
In0.52Al0.48As heterobarrier
  Carrier confinement
Semi-insulating InP
  Device isolation

## Slide 26: Gate First FET Process Flow
Front End: Gate Stack Definition
  In-situ hydrogen plasma / TMA treatment before Al2O3 growth
  Mixed e-beam / optical lithography
  Bi-layer gate (Sputtered W + e-beam evaporated Cr)
    High selectivity, low power dry etch

## Slide 27: FET Process Development
Use optical lithography to produce >0.5um gates
Use electron beam lithography to produce sub-100nm gates
Need to investigate possible e-beam damage to oxides
Cr
HSQ (SiO2)
W
Cr
SiO2
EBL Tests
Cr + SiNx
SiO2 + SiNx
W + SiNx
Field: SiNx
Finished Gate Etch + Sidewall Deposition

## Slide 28: FET Process Development
ICP dry etches calibrated to perform at sub-100nm scale
Increased ICP Power
Higher power dry etch  vertical gate stack
Undercutting leads to fallen gates, ungated access regions  Minimize Cr undercut by reducing thickness

## Slide 29: Gate First FET Process Flow
Front End: Gate Stack Definition
  Sidewall Deposition
    Conformal, protects S/D short circuit to gate
  Sidewall etch
    Vertical gate stack  self aligned sidewall

## Slide 30: FET Process Development
Low power etch  Isotropic etching + undercut  fallen gates
Large undercuts  ungated regions  high Raccess
Thick gate stack: Small Lg  Large sidewall foot  Unreliable gates 
Thin Cr stack: Small Lg  Large sidewall foot  Repeatable gate etch?
ALD SiO2 sidewall: Small Lg  Still sidewall foot!  Unrepeatable gate undercut 

## Slide 31: Gate First FET Process Flow
Regrowth and Back End
  Surface preparation
    UV O3 exposure to clean the source/drain, removed ex-situ before MBE load
  MBE InAs Regrowth
    Low arsenic flux, high temperature  near gate fill in
  Metallization and Mesa Isolation
    In-situ Mo in MBE optional for lower rc
    Ti/Pd/Au liftoff
    Wet etch for mesa isolation

## Slide 32: Gate First FET Process Flow
Regrowth
Regrowth
Tungsten
Chrome
SiO2
SiNx Sidewalls
TEM micrographs of 60 nm Lg device

## Slide 33: Gate First FET Results
60 nm Lg
115 nm Lg
Increased leakage current: Heavy d doping leakage path Drain induced barrier lowering

## Slide 34: Gate First FET Results
60 nm Lg
High Jdrain but depletion mode
Transconductance: Similar to previous results* (~0.3mS/mm)
Low Ron (371 ohm-mm) for InGaAs MOSFETs
1/Ron
*) U. Singisetti et al, IEEE EDL Nov. 2009.

## Slide 35: Gate First FET Results
Jdrain increases rapidly with gate length scaling
Transconductance: Relatively flat with gate length scaling
*) U. Singisetti et al, IEEE EDL Nov. 2009.
Wg = 9 mm

## Slide 36: FET: Access Resistance
Gateless transistor effective diagnostic of regrowth
MOSFET On Resistance
Gateless Transistor Resistance
Wg=9 mm Tchan=10 nm
Wg=25 mm Tchan=15 nm
Raccess: 200 ohm-mm
Raccess: 100 ohm-mm

## Slide 37: Gate First FET: Metal-Regrowth TLM
Metal-Regrowth access resistance
is not a limiting factor in Jdrain
Ex-situ Ti/Pd/Au / n-type InAs contacts: rc = 2 x 10-8 ohm-cm2
In-situ Mo / n-type InAs contacts have shown rc = 6 x 10-9 ohm-cm2 *
Wg = 14 mm
*) M.J.W. Rodwell, et al, IPRM 2010.

## Slide 38: Gate First FET: Issues
Ungated region  potential current choke
  Thinner sidewall can help…
  … but hard to control with gate undercut
Electron band diagram of channel underneath sidewall

## Slide 39: Gate First FET: Issues
Heavy d doping  parallel conduction, poor gm
  Large leakage current in device
  Decreases Cdepth  limits gm
Must reduce d doping while maintaining low Raccess

## Slide 40: FET Device Physics
Dit problem
  ↑Cit , ↓ Vsurface
  Vsurface also supplies Cdos
  ↓ Vsurface =↓ ndos in Cdos

## Slide 41
Rodwell, IPRM 2010
FET Device Scaling
FET parameters | Scaling Rule | How?
Current Density , gm | increase 2:1 | 
Gate Length and Contact Spacing (Lg,LS/D) | decrease 2:1 | Lithographic Scaling
Channel Electron Density | increase 2:1 | Channel Material and Orientation
Electron Transport Mass (m*transverse ) | constant | Channel Material and Orientation
Gate Capacitance | increase 2:1 | 
Channel Density of States | increase 2:1 | Channel Material and Orientation
Channel Thickness (Tinv) | decrease 2:1 | Materials Engineering
Effective Oxide Thickness (Tox) | decrease 2:1 | Materials Engineering
Source/Drain Contact Resistivity | decrease 4:1 | Materials Engineering

## Slide 42: FET Device Scaling
5 nm channel, 500 cm2/(V*s) mobility, 5E19 cm-3 carriers = 500 ohm/sq
5E-9 ohm cm2 contact resistance
Ltransfer ~ 31 nm
Contacted Gate Pitch
LS/D
Lg
WS/D
1) S. Natarajan, et al, IEDM 2008.
2) M.J.W. Rodwell, et al, IPRM 2010.

## Slide 43: FET Process Development
1) Poorly controlled dry etch undercut
  Low power etch  Isotropic etching
Thick gate stack: Small Lg  Large sidewall foot  unreliable gates 
Thin Cr stack: Small Lg  Large sidewall foot  Reliable gate etch?
ALD SiO2 sidewall: Small Lg  Still sidewall foot!  Unreliable gate undercut 