## Slide 1
12 nm-Gate-Length Ultrathin-Body InGaAs/InAs MOSFETs with 8.3∙105 ION/IOFF
Cheng-Ying Huang1, Prateek Choudhary1, Sanghoon Lee1, Stephan Kraemer2, Varistha Chobpattana2, Brain Thibeault1, William Mitchell1, Susanne Stemmer2, Arthur Gossard1,2, and Mark Rodwell1
1Electrical and Computer Engineering, University of California, Santa Barbara
2Materials Department, University of California, Santa Barbara
Device Research Conference 2015
Late News
Columbus, OH

## Slide 2: III-V FETs at sub-10-nm nodes?
III-V channels: low electron effective mass, high velocity, high mobility higher Ion at lower VDD reducing switching power
III-V FETs have high leakage current because:
Low bandgap larger band-to band tunneling (BTBT) leakage
High permittivity worse electrostatics, large subthreshold leakage
Ioff<100 nA/µm (High performance) and Ioff<100 pA/µm (Low power)
Question: Can III-V MOSFETs scale to sub-10-nm nodes?
2
Logic industry node | Physical gate length (nm)
16/14 | 20
10 | 17
7 | 14
5 | 12
Ref: 2013 ITRS Roadmap

## Slide 3: Record high performance III-V FETs
S. Lee et al., VLSI 2014
3
Vertical Spacer
N+ S/D
Lg~25 nm

## Slide 4: Record low leakage III-V FETs
4
Minimum Ioff~ 60 pA/μm at VD=0.5 V for Lg-30 nm
Recessed InP shows 100:1 smaller Ioff compared to InGaAs spacers
BTBT leakage is completely removed sidewall leakage dominates Ioff
Lg-30nm
C. Y. Huang et al., IEDM 2014
Lg-30nm

## Slide 5
UCSB Gate Last Process Flow
ZrO2
Barrier
Substrate
N+ S/D
Isolation
Strip dummy gate
Digital etch
Deposit ALD dielectric
FGA anneal
Ni
Barrier
Substrate
Lift-off gate metal
Ni
Barrier
Substrate
Ti/Pd/Au
Deposit
S/D contacts
HSQ
Barrier
Substrate
Pattern dummy gate
Source/drain recess etch
Channel
Barrier
Substrate
MBE grown device epilayer
MOCVD source/drain regrowth
5
Ch.
HSQ
Barrier
Substrate
N+ S/D
Ch.
Ch.
N+ S/D
N+ S/D
Ch.
Ch.

## Slide 6: TEM images of Lg~12 nm devices
N+InGaAs
InP spacer
InAlAs
Barrier
Lg~12nm
~ 8nm
6
tch~ 2.5 nm
(1.5/1 nm InGaAs/InAs)
Top View
Ni
Cross-setion
N+InP

## Slide 7: ID-VG and ID-VD curves of 12nm Lg FETs
7
Ioff~1.3 nA/μm
Ion~1.1 mA/μm
Ion/Ioff > 8.3∙105
Lg-12nm

## Slide 8: On-state performance
8
Slightly higher Gm for a 2.5 nm composite channel than a 4.5 nm InGaAs channel  larger gate capacitance.
A 2.5nm InAs channel with a 12 nm InGaAs spacer shows highest Gm  high indium content channel is desirable for UTB III-V FETs.
InP spacers increase parasitic RS/D to ~260 Ω∙μm  InP spacers need further optimization.

## Slide 9: Subthreshold characteristics
9
A 2.5nm InAs channel with a 12 nm InGaAs spacer shows the lowest SS and DIBL because of the best electrostatics.
A 5 nm un-doped InP spacer with the atop 8 nm linearly doping-graded InP have shorter effective gate length as compared to 12 nm un-doped InGaAs spacers worse electrostatics.
SS~107 mV/dec. and DIBL~260 mV/V for 12 nm devices FinFETs will cure this.

## Slide 10: Ion and Ioff versus Lg
10
High In% content channels are required to improve Ion, but Ioff is relatively large (~10 nA/µm).
InGaAs channels with recessed InP source/drain spacers are required for low leakage FETs.
A clear tradeoff between on-off performance.

## Slide 11: Mobility extraction at Lg-25 µm long channel FETs
Mobility~ 250 cm2/V∙s
Mobility~ 280 cm2/V∙s
Freq: 200 kHz
EOT~ 0.9~1 nm
This work
InAs channel
1.5/1 nm InGaAs/InAs
1.5/1 nm InGaAs/InAs
m*, RS/D more important!
11

## Slide 12: Summary
12
We demonstrated a 12nm-Lg ultrathin body III-V MOSFET with well-balanced on-off performance. (Ion/Ioff> 8.3·105)
The 12nm-Lg FET shows Gm~1.8 mS/µm and SS~107 mS/dec., and minimum Ioff~ 1.3 nA/µm.
High indium content channel is required to improve on-state current. (High performance logic)
Thin channels, InGaAs channels, and recessed InP source/drain spacers are the key design features for very low leakage III-V MOSFETs. (Low Power Logic)
III-V MOSFETs are scalable to sub-10-nm technology nodes.

## Slide 13
cyhuang@ece.ucsb.edu
Thanks for your attention! Questions?
This research was supported by the SRC Non-classical CMOS Research Center (Task 1437.009) and GLOBALFOUNDRIES(Task 2540.001).
A portion of this work was done in the UCSB nanofabrication facility, part of NSF funded NNIN network.
This work was partially supported by the MRSEC Program of the National Science Foundation under Award No. DMR 1121053.
Acknowledgment

## Slide 14
(backup slides follow)

## Slide 15: Record low subthreshold swing
15
Achieved SS~ 61 mV/dec.
Superior high-k dielectrics on III-V channels.
Dielectrics from Gift Chobpattana, Stemmer group, UCSB.
S. Lee et al., VLSI 2014

## Slide 16: Why InAs channel is better…
Electron scattering with oxide traps inside conduction band
Electrons in high In% content channel have less scattering with oxide traps.
J. Robertson et al., J. Appl. Phys. 117, 112806 (2015)
J. Robertson, Appl. Phys. Lett 94, 152104 (2009)
N. Taoka et al., Trans. Electron Devices. 13, 456 (2011)
N. Taoka et al., IEEE IEDM 2011, 610.

## Slide 17: InP spacer thickness: on-state
Thicker InP spacer increases Ron, and degrades Gm
Thinner spacer is desired at source to reduce RS/D.
17

## Slide 18: Doping-graded InP spacer
Doping-graded InP spacer reduces parasitic source/drain resistance and improves Gm.
Gate leakage limits Ioff~300 pA/μm.
18
Ron at zero Lg (Ω∙μm) | 5 nm UID InP | 13 nm UID InP | Doping graded InP
 | ~199 | ~364 | ~270
Lg-30 nm, 30Å ZrO2