## Slide 1: Prospects for Multi-THz III-V Transistors
Mark Rodwell, UCSB
J. Rode*, P. Choudhary*, B. Thibeault, W. Mitchell, A.C. Gossard : UCSB
* Now with Intel
M. Seo: Sungkyunkwan University
M. Urteaga, J. Hacker, Z. Griffith, B. Brar: Teledyne Scientific and Imaging
Workshop, WFH, “Microwave and Photonics Techniques for Terahertz Applications in Science and Technology”, IEEE-IMS Symposium, May 27, 2016, San Francisco

## Slide 2: Why mm-wave wireless ?

## Slide 3
Links

## Slide 4: mm-Waves: high-capacity mobile communications
Needs→ research: RF front end: phased array ICs, high-power transmitters, low-noise receivers IF/baseband: ICs for multi-beam beamforming, for ISI/multipath suppression, ...

## Slide 5: mm-Waves: benefits & challenges
Massive # parallel channels
Need mesh networks
Need phased arrays (overcome high attenuation)
5
Large available spectrum
line-of-sight MIMO
spatial multiplexing
(note high attenuation in foul weather)

## Slide 6: mm-Wave LOS MIMO: multi-channel for high capacity
Torklinson : 2006 Allerton Conference Sheldon : 2010 IEEE APS-URSI Torklinson : 2011 IEEE Trans Wireless Comm.

## Slide 7: Spatial Multiplexing: massive capacity RF networks
multiple independent beams each carrying different data each independently aimed # beams = # array elements
Hardware: multi-beam phased array ICs

## Slide 8: Millimeter-wave imaging
235 GHz video-rate synthetic aperture radar
10,000-pixel, 94GHz imaging array→ 10,000 elements
Golcuk: Trans MTT, Aug 2014
1 transmitter, 1 receiver 100,000 pixels 20 Hz refresh rate 5 cm resolution @ 1km 50 Watt transmitter (tube, solid-state driver)
Demonstrated: SiGe, 1.3 kW (UCSD/Rebeiz) Lower-power designs: InP, CMOS, SiGe (UCSB, UCSD, Virginia Poly.)

## Slide 9: 140 GHz, 10 Gb/s Adaptive Picocell Backhaul

## Slide 10: 140 GHz, 10 Gb/s Adaptive Picocell Backhaul
350 meters range in 50mm/hr rain
PAs: 24 dBm Psat (per element)→ GaN or InP
LNAs: 4 dB noise figure → InP HEMT
Realistic packaging loss, operating & design margins

## Slide 11: 340GHz, 160Gb/s spatially multiplexed backhaul
600 meters range in 50 mm/hr rain
1o beamwidth; 8o beamsteering
PAs: 14 dBm Psat (per element)→ InP
LNAs: 7 dB noise figure → InP HEMT
Realistic packaging loss, operating & design margins

## Slide 12: Optimum array size for low system power
At optimum-size array, target PA output power is typically 10-200 mW

## Slide 13: 50-500 GHz Wireless Transceiver Architecture
III-V LNAs, III-V PAs → power, efficiency, noise Si CMOS beamformer→ integration scale
...similar to today's cell phones.
backhaul
endpoint
High-gain antenna → large area → much too big for monolithic integration

## Slide 14
Transistors

## Slide 15: mm-wave CMOS (examples)
210 GHz amplifier: 32 nm SOI, positive feedback, 15 dB, 3 stages Wang et al. (Heydari), JSSC, March 2014
150 GHz amplifier: 65 nm bulk CMOS, 8.2 dB, 3 stages (250GHz fmax) Seo et al. (UCSB), JSSC, December 2009
300 GHz fmax

## Slide 16: mm-Wave CMOS won't scale much further
Gate dielectric can't be thinned → on-current, gm can't increase
Tungsten via resistances reduce the gain
Inac et al, CSICS 2011
Shorter gates give no less capacitance dominated by ends; ~1fF/mm total
Maximum gm, minimum C→ upper limit on ft. about 350-400 GHz.
Present finFETs have yet larger end capacitances

## Slide 17: III-V high-power transmitters, low-noise receivers
Cell phones & WiFi: GaAs PAs, LNAs
mm-wave links need high transmit power, low receiver noise
0.47 W @86GHz
0.18 W @220GHz
1.9mW @585GHz
M Seo, TSC, IMS 2013
T Reed, UCSB, CSICS 2013
H Park, UCSB, IMS 2014

## Slide 18: Scaling Laws, Scaling Roadmap
HBT parameter | change
emitter & collector junction widths | decrease 4:1
current density (mA/mm2) | increase 4:1
current density (mA/mm) | constant
collector depletion thickness | decrease 2:1
base thickness | decrease 1.4:1
emitter & base contact resistivities | decrease 4:1
Narrow junctions. Thin layers High current density Ultra low resistivity contacts
18

## Slide 19
Bipolar Transistor Design
19

## Slide 20
FET Design: Scaling
20

## Slide 21: THz HBTs: The key challenges
Obtaining good base contacts in HBT vs. in contact test structure (emitter contacts are fine)
Baraskar et al, Journal of Applied Physics, 2013
RC parasitics along finger length metal resistance, excess junction areas

## Slide 22: Emitter Length Effects: Decreased fmax
Results from finite-element modeling
On a 2 μm emitter finger, effect of base metal resistance can be comparable to adding 3 Ω-μm2 to the base contact resistivity !
base metal sheet resistance
22

## Slide 23: THz HBTs: double base metal process
Blanket surface clean (UV O3 / HCl) strips organics, process residues, surface oxides
Blanket base metal no photoresist; no organic residues Ru refractory diffusion barrier 2 nm Pt : penetrates residual oxides
Thick Ti/Au base pad metal liftoff thick metal→ low resistivity
Rode et al., IEEE TED, Aug. 2015

## Slide 24: Reducing Emitter Length Effects
small base post undercut
large base post
before
after
large base post undercut
small base post
24
Rode et al., IEEE TED, Aug. 2015
large emitter end undercut
small emitter end undercut

## Slide 25: Reducing Emitter Length Effects
before
after
thicker Au base metal
narrower collector junction
25
Rode et al., IEEE TED, Aug. 2015

## Slide 26
InP HBTs: 1.07 THz @200nm, ?? @ 130nm
?
Rode et al., IEEE TED, Aug. 2015

## Slide 27: 130nm /1.1 THz InP HBT: ICs to 670 GHz
614 GHz fundamental VCO
340 GHz dynamic frequency divider
620 GHz, 20 dB gain amplifier
M Seo, TSC IMS 2013
also: 670GHz amplifier J. Hacker , TSC IMS 2013 (not shown)
M. Seo, TSC / UCSB
M. Seo, UCSB/TSC IMS 2010
204 GHz static frequency divider (ECL master-slave latch)
Z. Griffith, TSC CSIC 2010
300 GHz fundamental PLL
M. Seo, TSC IMS 2011
220 GHz 180 mW power amplifier
T. Reed, UCSB CSICS 2013
600 GHz Integrated Transmitter PLL + Mixer
M. Seo TSC
Integrated 300/350GHz Receivers: LNA/Mixer/VCO
M. Seo TSC
81 GHz 470 mW power amplifier
H-C Park UCSB IMS 2014

## Slide 28: Towards a 3 THz InP Bipolar Transistor
Extreme base doping→ low-resistivity contacts→ high fmax
Extreme base doping→ fast Auger (NP2) recombination→ low b.
Solution: very strong base compositional grading→ high b

## Slide 29: Towards a 3 THz InP Bipolar Transistor
ALD metal process: form 32 nm emitter contact
Extreme base grading (alloy, bandgap)
high surface doping: good contacts, low b extreme grading→ recovers b

## Slide 30: First Step: the ALE-defined Emitter

## Slide 31: 1/2-THz SiGe HBTs
500 GHz fmax SiGe HBTs Heinemann et al. (IHP), 2010 IEDM
16-element multiplier array @ 500GHz (1 mW total output) U. Pfeiffer et. al. (Wuppertal / IHP) , 2014 ISSCC

## Slide 32: Towards a 2 THz SiGe Bipolar Transistor
 | InP | SiGe | 
emitter |  |  | 
junction width | 64 | 18 | nm
access resistivity | 2 | 0.6 | W-mm2
base |  |  | 
contact width | 64 | 18 | nm
contact resistivity | 2.5 | 0.7 | W-mm2
collector |  |  | 
thickness | 53 | 15 | nm
current density | 36 | 125 | mA/mm2
breakdown | 2.75 | 1.3? | V
ft | 1000 | 1000 | GHz
fmax | 2000 | 2000 | GHz
Similar scaling InP: 3:1 higher collector velocity SiGe: good contacts, buried oxides
Key distinction: Breakdown
InP has: thicker collector at same ft, wider collector bandgap
Key requirements:
low resistivity Ohmic contacts note the high current densities
Assumes collector junction 3:1 wider than emitter.
Assumes SiGe contacts no wider than junctions

## Slide 33
FET scaling laws; 2:1 higher bandwidth | change
gate length | decrease 2:1
current density (mA/mm), gm (mS/mm) | increase 2:1
transport mass | constant
gate-channel capacitance density | increase 2:1
contact resistivities | decrease 4:1
Towards at 2.5 THz HEMT
Xiaobing Mei, et al, IEEE EDL, April 2015 (Northrop-Grumman)
First Demonstration of Amplification at 1 THz Using 25-nm InP High Electron Mobility Transistor Process
Need thinner dielectrics, better contacts

## Slide 34
FET Scaling Laws (these now broken)
fringing capacitance does not scale → linewidths scale as (1 / bandwidth )
34
FET parameter | change
gate length | decrease 2:1
current density (mA/mm) | increase 2:1
transport mass | constant
2DEG electron density | increase 2:1
gate-channel capacitance density | increase 2:1
dielectric equivalent thickness | decrease 2:1
channel thickness | decrease 2:1
channel state density | increase 2:1
contact resistivities | decrease 4:1

## Slide 35: Record III-V MOS
S. Lee et al., VLSI 2014
Vertical Spacer
N+ S/D
Lg~25 nm
record for III-V
= best UTB SOI silicon

## Slide 36: Excellent III-V gate dielectrics
61 mV/dec Subthreshold swing at VDS=0.1 V
Negligible hysteresis
2.5nm ZrO2 1nm Al2O3
2.5nm InAs
V. Chobpattanna, S. Stemmer FET data: S Lee, 2014 VLSI Symp.

## Slide 37: III-V MOS @ Lg = ???
Image courtesy of S. Kraemer (UCSB)
Huang et al., 2015 DRC

## Slide 38: Towards at 2.5 THz HEMT
C. Y. Huang et al., DRC 2015
VLSI III-V MOS
THz III-V MOS

## Slide 39
Power Amplifiers

## Slide 40: 220 GHz power amplifiers; 256nm InP HBT
90 mW
180 mW (330 mW design; thermally limited)
164 mW, 0.43 W/mm, 2.4% PAE
T. Reed (UCSB), Z. Griffith (TSC), IEEE CSIC 2012 & 2013; Teledyne 256nm InP HBT

## Slide 41: mm-Wave Power Amplifier: Challenges
needed: High power / High efficiency / Small die area ( low cost)
Extensive power combining
Compact power-combining
Efficient power-combining
Class E/D/F are poor @ mm-wave insufficient fmax , high losses in harmonic terminations
Goal: efficient, compact mm-wave power-combiners

## Slide 42: Parallel Power-Combining
Output power: POUT = N x V x I Parallel connection increases POUT
Load Impedance: ZOPT = V / (N x I) Parallel connection decreases Zopt
High POUT→ Low Zopt
Needs impedance transformation: lumped lines, Wilkinson, ...
High insertion loss Small bandwidth Large die area

## Slide 43: Series Power-Combining & Stacks
Parallel connections: Iout=N x I Series connections: Vout=N x V
Local voltage feedback: drives gates, sets voltage distribution
Design challenge: need uniform RF voltage distribution need ~unity RF current gain per element
...needed for simultaneous compression of all FETs.
Output power: Pout=N2 x V x I Load impedance: Zopt=V/I Small or zero power-combining losses Small die area How do we drive the gates ?
Shifrin et al., 1992 IEEE-IMS; Rodwell et al., U.S. Patent 5,945,879, 1999; Pornpromlikit et al., 2011 CSICS

## Slide 44: Sub-λ/4 Baluns for Series Combining
Sub-l/4 balun : stub→ inductive tunes transistor Cout ! short lines→ low losses short lines → small die
Standard l/4 balun : long lines → high losses → large die
Balun combiner: 2:1 series connection each source sees 25 W → 4:1 increased Pout
Park et al., 2013 CSICS, 2014 IEEE-IMS

## Slide 45: 2:1 series-connected 86GHz power amplifier
Daneshgar et al., 2014 IEEE-IMS
20 dB Gain 188mW Psat 1.96 W/mm 32.8% PAE Teledyne 250 nm InP HBT 2 stages, 1.0 mm2

## Slide 46: 4:1 series-connected 81GHz power amplifier
17 dB Gain 470 mW Psat 23% PAE Teledyne 250 nm InP HBT 2 stages, 1.0 mm2(incl pads)
Park et al., 2014 IEEE-IMS

## Slide 47: Teledyne: 1.9 mW, 585 GHz Power Amplifier
Output Power
12-Stage Common-base
2.8 dBm Psat
>20 dB gain up to 620 GHz
What limits output power in sub-mm-wave amplifiers ?
S-parameters
M. Seo et al., Teledyne Scientific: IMS2013

## Slide 48: Sub-mm-wave PAs: need more current !
common-base HBT
base
emitter
collector
ground plane
HBTs with microstrip combiner
3 mm max emitter length (> 1 THz fmax) 2 mA/mm max current density Imax= 6 mA Maximum 3 Volt p-p output Load: 3V/6mA= 500 W
Combiner cannot provide 500 W loading

## Slide 49: Multi-finger HBTs: more current, lower fmax
More current → lower cell load resistance
one-finger common-base HBT
two-finger power cell
four-finger power cell: parasitics
base
emitter
collector
ground plane
base
emitter
collector
base
emitter
collector
unequal emitter inductances
emitter-collector capacitance
Reduced fmax, reduced RF gain: common-lead inductance→ Z12 feedback capacitance→ Y12 phase imbalance between fingers.
Worse at higher frequencies: less tolerant of cell parasitics less current per cell higher required load resistance Can optimum load be reached ?

## Slide 50: Sub-mm-wave transistors: need more current
InP HBTs: thinner collector→ more current hotter→ improve heat-sinking or: longer emitters→ thicker base metal
GaN HEMTs: much higher voltage 100+ GHz: large multi-finger FETs not feasible Need high current to exploit high voltage.
Need more mA/mm or longer fingers
Example: 2mA/mm, 100 mm max gate width, 50 Volts 200mA maximum current 50 Volts/200mA= 250 W load→ unrealizable.

## Slide 51
50-500GHz Wireless

## Slide 52: 50-500 GHz Wireless Electronics
Mobile communication @ 2Gb/s per user, 1 Tb/s per base station
Requires: large arrays, complex signal processing, high Pout , low Fmin
VLSI beamformers VLSI equalizers III-V LNAs & PAs
III-V Transistors may perform well enough even for 1 THz systems.

## Slide 53
(backup slides follow)