## Slide 1: Future Directions in > 100 GHz Devices
Mark Rodwell, Yihao Fang, Brian Markman, Hsin-Ying Tseng University of California, Santa Barbara rodwell@ece.ucsb.edu
This work was supported in part by the Semiconductor Research Corporation (SRC), DARPA, and the NSF
2019 IEEE SISC Conference, December 13, San Diego

## Slide 2: Future Directions in > 100 GHz Devices
Mark Rodwell, Yihao Fang, Brian Markman, Hsin-Ying Tseng University of California, Santa Barbara rodwell@ece.ucsb.edu
This work was supported in part by the Semiconductor Research Corporation (SRC), DARPA, and the NSF
2019 IEEE SISC Conference, December 13, San Diego
Materials Requirements for Future Transistors

## Slide 3: Transistor design and materials requirements
Transistors for VLSI Large Ion, small Ioff, low VDD, small footprint… hard ! MOSFETs, TFETs.
Transistors for wireless High (ft,fmax) , low noise, high power, high efficiency. InP HBTs, InP MOS-HEMTs, (GaN HEMTs, SiGe HBTs)
Transistors for power switching: high speed, high voltage, high current, GaN, SiC, Si LDMOS …not my field.

## Slide 4
nm FETs: MOS and TFETs

## Slide 5: MOSFETs for VLSI
Goals: large Ion, small Ioff, low VDD, small footprint Minimum Lg set by minimum equivalent oxide thickness. ZrxHf1-xO2 ? Minimum contact size set by contact resistivity (<0.3 W-mm2) Ballistic Ion set by band structure: EOT, m*, # valleys Ioff is degraded by low bandgap Ideal: m*=0.1me, 2-3 valleys, Eg>1eV, grades to small-Eg contact layers

## Slide 6: High-current triple-heterojunction TFETs for VLSI
TFETs: steep SS , low Ion; ✘ Triple-HJ TFET: steep SS , high Ion; 
Materials needs: Direct bandgap, large band offsets, small tunnel barrier, low m* Low Dit for N & P materials. (N-InAs , N-InP , P-GaAsSb ?, P-InGaAs ?) small dielectric EOT, low r contacts
< 2nm barrier
Simulations: M. Povoloski, Purdue

## Slide 7
High-Frequency Transistors

## Slide 8: Beyond-5G Wireless: 100-300GHz
10Gb mobile communications: Unlimited information, anywhere. Capacity well beyond 5G.
TV-resolution wireless imaging: See, fly, drive perfectly in any conditions.
Debdeep Jena, Alyosha Molnar, Christoph Studer, Huili Xing: Cornell University
Dina Katabi: MIT
Sundeep Rangan: New York University
Amin Arbabian, Srabanti Chowdhury: Stanford
Elad Alon, Ali Niknejad, Borivoje Nikolic, Vladimir Stojanovic: University of California, Berkeley
Gabriel Rebeiz: University of California, San Diego
Jim Buckwalter, Upamanyu Madhow, Umesh Mishra, Mark Rodwell: University of California, Santa Barbara
Andreas Molisch, Hossein Hashemi: University of Southern California
Harish Krishnaswamy: Columbia University
Kenneth O: University of Texas, Dallas

## Slide 9: Target applications
MIMO hub: 140GHz, 128 beams/face, 10Gb/s/user, 100m
Point-point MIMO: 240GHz, 340GHz: 640Gb/s, 250-500m
Hardware-efficient imaging: 240GHz, 340 GHz, 300m, 512×64 image, 60Hz, 15dB SNR
5 Tb/s !

## Slide 10: A few high-frequency ICs
570 GHz fundamental oscillator; InP HBT
M. Seo, TSC / UCSB JSSC, 2011
600 GHz Integrated Transmitter; InP HBT PLL + Mixer+Amplifier
M. Seo TSC 2012 IMS
204 GHz static frequency divider (ECL master-slave latch); InP HBT
Z. Griffith, TSC / UCSB CSIC 2010
1.0 THz Amplifier; InP HEMT
Mei et al, Northrop-Grumman EDL, 2015
220 GHz 180 mW power amplifier; InP HBT
T. Reed, UCSB Z. Griffith, TSC CSICS 2013

## Slide 11: Transistor development for 100-300GHz systems
THz InP HBTs: Efficient 100-650GHz power more fmax: more efficient, higher frequencies base regrowth: better contacts→ higher fmax. status: working DC devices; moving to THz
THz InP HBTs: Sensitive 100-650GHz low-noise amplifiers more ft: lower noise, higher frequencies high-K gate dielectric → higher ft. status: process modules
InGaN and GaN HEMTs: High power from 100-340GHz GaN: superior power density at all frequencies UCSB/Mishra: InGaN for increased mobility Cornell/Xing: AlN/GaN/AlN
N-polar GaN: Mishra, UCSB

## Slide 12: Transistor scaling laws: ( V,I,R,C,t ) vs. geometry
Bulk and Contact Resistances
Depletion Layers
Thermal Resistance
Fringing Capacitances
Available quantum states to carry current
→ capacitance, transconductance contact resistance

## Slide 13: Degenerate State Density (Ballistic) Limits

## Slide 14
Frequency Limits and Scaling Laws of (most) Electron Devices
To double bandwidth: Reduce thicknesses 2:1 Improve contacts 4:1 Reduce width 4:1, Keep constant length Increase current density 4:1
PIN photodiode

## Slide 15
THz Bipolar Transistors

## Slide 16: Bipolar Transistor Design: Scaling

## Slide 17: Bipolar Transistor Scaling Laws
Narrow junctions. Thin layers High current density Ultra low resistivity contacts

## Slide 18
InP HBTs: 1.07 THz @200nm
?
Rode et al., IEEE TED, Aug. 2015

## Slide 19: Challenges at the 64nm/2THz & 32nm/3THz Nodes
Baraskar et al, Journal of Applied Physics, 2013
Need high base contact doping >1020/cm3 for good contacts high Auger recombination very low b.
Need moderate contact penetration Pd or Pt contacts react with 3++ nm of base penetrate surface contaminants too deep for thin base
Solution: base regrowth: thin, moderately-doped intrinsic base InGaAs or GaAsSb @ 1019-1020/cm3 thick, heavily-doped extrinsic base P-GaAs, ~1021/cm3
Rode et al., IEEE TED, Aug. 2015

## Slide 20: Regrown-Base InP HBTs: Images
Cross-sections
Dry-etched TiW emitter contact

## Slide 21: Regrown-Base InP HBTs: Status
Excellent base contacts; but hydrogen base passivation 0.4 W-mm2 resistivity for GaAs/metal contact 290 W sheet resistivity for regrown base  0.60W-mm2 resistivity for InGaAs/GaAs contact✘ 1940W/ sheet resistivity for intrinsic base ✘
Good DC data: even given regrowth refractory Mo/W/TiW emitter contact maintains low rc.
Current process runs: GaAsSb intrinsic base resistant to hydrogen passivation of carbon base dopant (current reference sample: GaAsSb base, no regrowth)→→

## Slide 22: Materials for Improved THz HBTs
Contacts: existing materials are sufficient. N-InAs for emitter, regrown ~1021 cm-3 GaAs for base
Base transit time is no problem: regrowth permits very thin base
Desire: improved voltage at a given bandwidth 1.4eV bandgap→ 30V/mm breakdown But: increased transit time at high Vce: G-(L,X) scattering, E-k dispersion
Is there a better collector material ?: Larger bandgap Larger G-(L,X) energy separation Low optical phonon scattering rates (GaN suffers here). High thermal conductivity.
Prof. Jasprit Singh; eecs320 notes, Univ Michigan;

## Slide 23
THz Field-Effect Transistors

## Slide 24: FETs (HEMTs): key for low noise
2:1 to 4:1 increase in ft : improved noise less required transmit power smaller PAs, less DC power
or higher-frequency systems

## Slide 25: High-Frequency FET Scaling
To double ft , reduce Lg 2:1, but this is not enough
Must also reduce Cgsx/gm , Cgd/gm time constants 2:1
→ gm/Wg must be doubled
Must also thin dielectric and channel by 2:1 (gmRds)

## Slide 26: FET Current and Transconductance
To increase gm: thin the oxide & channel and increase K1 (mass, # valleys)…hard or increase (Vgs-Vth)…also hard

## Slide 27: FET Scaling Laws (these now broken)
FET parameter | change
gate length | decrease 2:1
current density (mA/mm) | increase 2:1
specific transconductance (mS/mm) | increase 2:1
transport mass | constant
2DEG electron density | increase 2:1
gate-channel capacitance density | increase 2:1
dielectric equivalent thickness | decrease 2:1
channel thickness | decrease 2:1
either (channel state density) | increase 2:1
or (Vgs-Vth) | increase 4:1
contact resistivities | decrease 4:1
Gate dielectric can't be much further scaled. Not in CMOS VLSI, not in mm-wave HEMTs
gm/Wg (mS/mm) hard to increase→ Cend / gm prevents ft scaling.
Shorter gate lengths degrade electrostatics→ reduced gm /Gds → reduced fmax , ft

## Slide 28
Towards faster HEMTs: InAs MOS-HEMTs
Scaling limit: gate insulator thickness HEMT: InAlAs barrier: tunneling, thermionic leakage solution: replace InAlAs with high-K dielectric 2nm ZrO2 (er=25): adequately low leakage
Scaling limit: source access resistance HEMT: InAlAs barrier is under N+ source/drain solution: regrowth, place N+ layer on InAs channel Target ~10nm node ~0.3nm EOT, 3nm thick channel 1.2 to 1.5 THz ft.
8/2019: process working: 470GHz ft. @ ~28nm Lg. fmax very low, ft high but not high enough. Now fixing obvious process problems.
1st MOS-HEMT demonstration: Fraunhofer IAF

## Slide 29: Device Images

## Slide 30: More Device Images

## Slide 31: Increasing FET transconductance
For 1-2 THz ft , seek gmi= 4-8 mS/mm. thin the oxide, thin the well → increased eigenstate energy → loss of confinement at large (Vgs-Vth) → constrains maximum transconductance: gm∝(Vgs-Vth)1/2 → maximum achievable gm.
Need high barrier energies InAs/InAlAs vs InAs/AlAsSb InP/AlAsSb ????
Huang, JAP, 2014
B. Markman, to be published

## Slide 32: mm-Wave CMOS also won't scale much further
High-frequency Si MOSFET design follows the same principles as high-frequency III-V FET design. Same physics, so same limits. But, the carrier velocities are lower
Difficult to further thin the gate dielectric (increased gate leakage)→ gm can't increase
Shorter gates don't significantly reduce the capacitance: dominated by ends; ~1fF/mm total
Maximum gm, minimum C→ upper limit on ft. about 350-400 GHz. At the *bottom* of the wiring stack
Usable bandwidth is lower than this high-frequency circuits need controlled-impedance Zo=50W interconnects microstrip lines with signal lines at top of wiring stack. high-frequency transistors must interface to ~50 Ohm external impedances ~20-30 FET fingers must be tied in parallel to bring device port impedances close to 50W. The necessary wiring further reduces ft, fmax: c.a. 300GHz in leading CMOS technologies.
The best CMOS node for mm-wave is 65nm. 45nm SOI, 22nm SOI are close to this performance Intel's RF-optimized 22nm finFET is also close to this performance

## Slide 33: Materials for THz (MOS) HEMTs
Low resistance in source-gate access region: moderate to high mobility
High transconductance sufficient mobility to reach ballistic current. m*≈ 0.08·mo to 0.16·mo high ballistic vinj desirable/hard: multiple band minima (large ns) large band offsets for large (Ef-Ec)→ large (Vgs-Vth)
Low S/D access resistances S/D materials with high doping, low barriers. Grade heterointerfaces
High velocities and high breakdown fields in gate-drain drift region m* need not be particularly low low phonon scattering rates large intervalley energy separation wide bandgap

## Slide 34
Closing

## Slide 35: Materials Requirements for Future Transistors
VLSI (MOSFETs, TFETs): It's mostly about the interfaces: gate dielectrics, S/D contacts The channel also matters: high ballistic Ion, sufficient Eg for low Ioff
MOS-HEMTs for mm-wave ICs, 50-500GHz low-noise amplifiers Same as VLSI MOSFETs: gate dielectrics, S/D contacts Large ballistic Ion. How to increase gm ? Large (Vgs-Vth)→ large (Ebarrier-Ewell)
HBTs for mm-wave ICs, 50-500 GHz power Contacts are critically important…and achievable Breakdown vs. transit time: ballistic overshoot matters. Large intervalley separation, low scattering rates

## Slide 36
In case of questions

## Slide 37
FET Design: Scaling