## Slide 1: Beyond 5G: 100-340GHz Transistor, IC, and System Design
Mark Rodwell, University of California, Santa Barbara
Short Course: Device Research Conference, June 23, 2019, University of Michigan

## Slide 2: ComSenTer: Wireless Research
Center for Converged Communications & Sensing at THz.
Duration: 5-years; 1/2018-12/2022.
Funding: about $36 million total.
Team: 21 Professors, ~65 Ph.D. students
Sponsors: SRC, DARPA
Focus: wireless systems, 10-15 years out, 100-340GHz

## Slide 3: Wireless above 100GHz
Wireless networks: exploding demand.
Immediate industry response: 5G. 28, 38, 57-71(WiGig), 71-86GHz increased spectrum, extensive beamforming
Next generation (6G ??): above 100GHz.. greatly increased spectrum, massive spectral multiplexing
DOD applications: Imaging/sensing/radar, comms.

## Slide 4: 140-340GHz Wireless
10Gb mobile communications: Unlimited information, anywhere. Capacity well beyond 5G.
TV-resolution wireless imaging: See, fly, drive perfectly in any conditions.

## Slide 5: Benefits of Short Wavelengths
Communications: Massive spatial multiplexing, massive # of parallel channels
Imaging: very fine angular resolution
But: High losses in foul or humid weather. High l2/R2 path losses. ICs: poorer PAs & LNAs. Beams easily blocked.
100-340GHz wireless: terabit capacity, short range, highly intermittent

## Slide 6: mm-waves: benefits & challenges
Massive # parallel channels
Need mesh networks
Need phased arrays (overcome high attenuation)
Large available spectrum
line-of-sight MIMO
spatial multiplexing
(note high attenuation in foul or humid weather)
Torklinson : 2006 Allerton Conference Sheldon : 2010 IEEE APS-URSI Torklinson : 2011 IEEE Trans Wireless Comm.

## Slide 7
140-340 GHz: Applications

## Slide 8: 140 GHz spatially multiplexed base station
1 Tb/s spatially-multiplexed base station 256 users/face, 4 faces 1024 total users @ 1 user/beam, 1 Gb/s/beam; 225 m range
Link budget is feasible, but... Required component dynamic range ? Required complexity of back-end beamformer ?
Handset: 8 × 8 array (9×9mm)

## Slide 9: 140 GHz spatially multiplexed base station
Each face supports 256 beams @ 1Gb/s/beam.
225 meters range in 50 mm/hr rain
PAs: 16 dBm Pout (per element)
LNAs: 3 dB noise figure
Realistic packaging loss, operating & design margins (20dB total)

## Slide 10: 75 GHz spatially multiplexed base station
If we use instead a 75GHz carrier, but constrain the handset to a similar size (8mm×8mm) and the hub to the same number of elements then the range becomes 210 meters (vs. 225 meters)
*The hub array is now 9mm×655mm (vs. 5mm×350mm)
Would be similar performance; except that PAs, LNAs are poorer @ 140GHz

## Slide 11: 340 GHz (or even 650 GHz) backhaul
Sub-mm-wave line-of-sight MIMO network backbone wireless @ optical speed; link network where fiber is too expensive to place. 340 GHz: 640Gb/s @ 500 meters range; 1.6 meter linear array (5Tb/s for 8×8 square array). 650 GHz: 1.28Tb/s @ 500 meter range; 1.6 meter linear array. Capacity doubles again if we use both polarizations.
linear array
square array

## Slide 12: 340 GHz 640 Gb/s MIMO backhaul
1.6m MIMO array: 8-elements, each 80 Gb/s QPSK; 640Gb/s total 4 × 4 sub-arrays → 8 degree beamsteering
500 meters range in 50 mm/hr rain; 29 dB/km
PAs: 82mW Pout (per element)
LNAs: 4 dB noise figure
Realistic packaging loss, operating & design margins

## Slide 13: 340 GHz 5 Tb/s MIMO backhaul
8-element 640Gb/s linear array: requires 80mW power/element requires 1.6m linear array
8-element 5Tb/s square array: same link assumptions requires 10mW power/element ...10W total radiated power requires 1.6m square array
500m range in 50mm/hr. rain.

## Slide 14: 140 GHz, 640 Gb/s MIMO backhaul
8-element 640Gb/s linear array: same link assumptions requires 2mW (vs. 80mW) power/element requires 2.6m (vs. 1.6m) linear array
Why not use a lower-frequency carrier, e.g. 140 GHz ?
8-element 5Tb/s square array: same link assumptions requires 0.25mW (vs. 10mW) power/element requires 2.6m (vs. 1.6m) square array

## Slide 15: High-resolution imaging radar
Proposed demo: 220GHz frequency-scanned system 64×512 pixels, 60Hz refresh 35cm × 35cm aperture 64-element linear array Target: 0.3m diameter, 10% reflectivity, 300m range detect with 5dB SNR in 35dB/km fog. System: F=6dB, Pelement= 10dBm (10% duty cycle)
DOD-relevant: 140GHz close-range system 256×256 pixels, 10ms image acquisition time 27 cm linear arrays, 256 elements Target (large bullet): 2cm diameter , 10% reflectivity, 100m detect with 10dB SNR in 20dB/km rain. System F=6dB, → Need 0.4W PAs (10% duty cycle) (reasonable margins)

## Slide 16
Systems

## Slide 17: Beamforming for massive spatial multiplexing
Pure digital beamforming: dynamic range & phase noise requirements: appear to be manageable  Digital back-end processing requirements (die area, DC power): being investigated ???
Pure RF beamforming: (focal plane, Butler matrixes, RF beamforming) Established approach in DOD systems (high dynamic range). Issues of array tiling.

## Slide 18: Beamforming for massive spatial multiplexing
ADCs/DACs: only 3-4 bit ADC/DACs required (Madhow, Studer, Rodwell)
Linearity: Amplifier P1dB need be only 3dB above average power (Madhow).
Phase noise: Requirements same as for SISO (Alon, Madhow, Niknejad, Rodwell)
Efficient digital beamforming: beamspace algorithm=complexity ~N× log(N) (Madhow)
Efficient digital beamforming: low-resolution matrix (Studer)
Efficient channel estimation : fast beamspace algorithm (Studer)
Efficiently addressing true-time-delay problem: "rainbow" FFT algorithm (Madhow)
Array-to-backplane interconnect power: low-power analog baseband 50W links (Rodwell)
Digital beamforming
In progress…
Propagation models and measurements: (Molisch)
Blockage probability, mesh networks, network protocols: (Rangan, Cabric)
MIMO system power analysis: (Rangan, Cabric, Buckwalter)

## Slide 19
Transistors

## Slide 20: mm-Wave Wireless Transceiver Architecture
custom PAs, LNAs → power, efficiency, noise Si CMOS beamformer→ integration scale
...similar to today's cell phones.

## Slide 21: IC Technologies for 100 + GHz systems
Silicon baseband processing at all frequencies RF sections @ 140, 200GHz PAs, LNAs in short-range 140, 220 GHz links GaN high-power amplifiers in long-range 140,220GHz links (possibly 340GHz ?)
InP HEMT low-noise amplifiers in long-range 140,220GHz links low-noise amplifiers @ 340, 650GHz
InP HBT medium-power amplifiers in long-range 140,220GHz links power amplifiers @340, 650GHz RF sections @ 340, 650GHz
Point-point MIMO: 340GHz: F= 4dB, Pavg=9.9dBm, Psat≅13.9dBm 650GHz: F= 4dB, Pavg=14.5dBm, Psat≅18.5dBm?
MIMO hub: 140GHz: F= 4dB, Pavg=17.5dBm, Psat≅21.5dBm 220GHz: F= 4dB, Pavg=21dBm, Psat≅25dBm

## Slide 22: mm-wave CMOS (UCSB examples)
150 GHz amplifier: IBM 65 nm bulk CMOS, 2.7dB gain per stage Seo et al., JSSC, Dec. 2009
145 GHz amplifier GF 45 nm SOI CMOS, 6.3 dB gain per stage Kim, Simseck, 2017 BCICTS

## Slide 23: mm-Wave CMOS won't scale much further
Gate dielectric can't be thinned → on-current, gm can't increase
Tungsten via resistances reduce the gain
Inac et al, CSICS 2011
Shorter gates give no less capacitance dominated by ends; ~1fF/mm total
Maximum gm, minimum C→ upper limit on ft. about 350-400 GHz.
Present finFETs have yet larger end capacitances

## Slide 24: III-V high-power transmitters, low-noise receivers
Cell phones & WiFi: GaAs PAs, LNAs
mm-wave links need: high transmit power, low receiver noise
0.47 W @86GHz
0.18 W @220GHz
1.9mW @585GHz
M Seo, TSC, IMS 2013
T Reed, UCSB, CSICS 2013
H Park, UCSB, IMS 2014

## Slide 25: Gallium Nitride Power Technologies
N-polar GaN: Mishra
GaN is the leading high-frequency power technology

## Slide 26: 130nm / 1.1THz InP HBT Technology
Teledyne: M. Urteaga et al: 2011 DRC
Rode (UCSB), IEEE TED, 2015
3.5 V breakdown

## Slide 27: 130nm / 1.1THz InP HBT: IC Examples
Teledyne: M. Urteaga et al: 2017 IEEE Proceedings
Integrated ~600GHz transmitter
220 GHz 0.18W power amplifier
UCSB/Teledyne: T. Reed et al: 2013 CSICS
325 GHz, 16mW power amplifier
UCSB/Teledyne: A. Ahmed, 2018 EuMIC Symp.
but, only ~1 mW output power

## Slide 28: Transistor scaling laws: ( V,I,R,C,t ) vs. geometry
Bulk and Contact Resistances
Depletion Layers
Thermal Resistance
Fringing Capacitances
Available quantum states to carry current
→ capacitance, transconductance contact resistance

## Slide 29
Frequency Limits and Scaling Laws of (most) Electron Devices
To double bandwidth: Reduce thicknesses 2:1 Improve contacts 4:1 Reduce width 4:1, Keep constant length Increase current density 4:1
PIN photodiode

## Slide 30: Bipolar Transistor Design

## Slide 31: Bipolar Transistor Design: Scaling

## Slide 32: Making faster bipolar transistors
to double the bandwidth: | change
emitter & collector junction widths | decrease 4:1
current density (mA/mm2) | increase 4:1
current density (mA/mm) | constant
collector depletion thickness | decrease 2:1
base thickness | decrease 1.4:1
emitter & base contact resistivities | decrease 4:1
Narrow junctions. Thin layers High current density Ultra low resistivity contacts
Teledyne: M. Urteaga et al: 2011 DRC

## Slide 33
InP HBTs: 1.07 THz @200nm, ?? @ 130nm
?
Rode et al., IEEE TED, Aug. 2015

## Slide 34: THz HBTs: The key challenges
Obtaining good base contacts in HBT vs. in contact test structure (emitter contacts are fine)
Baraskar et al, Journal of Applied Physics, 2013
RC parasitics along finger length metal resistance, excess junction areas

## Slide 35: Towards a 2 THz SiGe Bipolar Transistor
 | InP | SiGe | 
emitter |  |  | 
junction width | 64 | 18 | nm
access resistivity | 2 | 0.6 | W-mm2
base |  |  | 
contact width | 64 | 18 | nm
contact resistivity | 2.5 | 0.7 | W-mm2
collector |  |  | 
thickness | 53 | 15 | nm
current density | 36 | 125 | mA/mm2
breakdown | 2.75 | 1.3? | V
ft | 1000 | 1000 | GHz
fmax | 2000 | 2000 | GHz
Similar scaling InP: 3:1 higher collector velocity SiGe: good contacts, buried oxides
Key distinction: Breakdown
InP has: thicker collector at same ft, wider collector bandgap
Key requirements:
low resistivity Ohmic contacts note the high current densities
Assumes collector junction 3:1 wider than emitter.
Assumes SiGe contacts no wider than junctions

## Slide 36: FETs (HEMTs): key for low noise
2:1 to 4:1 increase in ft : improved noise less required transmit power smaller PAs, less DC power
or higher-frequency systems

## Slide 37: InP HEMTs: state of the art
Xiaobing Mei, et al, IEEE EDL, April 2015 (Northrop-Grumman)
First Demonstration of Amplification at 1 THz Using 25-nm InP High Electron Mobility Transistor Process

## Slide 38: FET Scaling Laws (these now broken)
FET parameter | change
gate length | decrease 2:1
current density (mA/mm) | increase 2:1
specific transconductance (mS/mm) | increase 2:1
transport mass | constant
2DEG electron density | increase 2:1
gate-channel capacitance density | increase 2:1
dielectric equivalent thickness | decrease 2:1
channel thickness | decrease 2:1
channel state density | increase 2:1
contact resistivities | decrease 4:1

## Slide 39: FET Scaling Laws (these now broken)
FET parameter | change
gate length | decrease 2:1
current density (mA/mm) | increase 2:1
specific transconductance (mS/mm) | increase 2:1
transport mass | constant
2DEG electron density | increase 2:1
gate-channel capacitance density | increase 2:1
dielectric equivalent thickness | decrease 2:1
channel thickness | decrease 2:1
channel state density | increase 2:1
contact resistivities | decrease 4:1
Gate dielectric can't be much further scaled. Not in CMOS VLSI, not in mm-wave HEMTs
gm/Wg (mS/mm) hard to increase→ Cend / gm prevents ft scaling.
Shorter gate lengths degrade electrostatics→ reduced gm /Gds → reduced fmax , ft

## Slide 40
Towards faster HEMTs: MOS-HEMTs
Scaling limit: gate insulator thickness HEMT: InAlAs barrier: tunneling, thermionic leakage solution: replace InAlAs with high-K dielectric 2nm ZrO2 (er=25): adequately low leakage
Scaling limit: source access resistance HEMT: InAlAs barrier is under N+ source/drain solution: regrowth, place N+ layer on InAs channel Target ~10nm node ~0.3nm EOT, 3nm thick channel 1.2 to 1.5 THz ft.
Jun Wu, UCSB, IEEE EDL, 2018

## Slide 41
ICs

## Slide 42: mm-Wave IC design: the challenges
Transistor gains are low: fsignal is significant fraction of fmax. match for optimum gain, noise, or power.
Device dimensions are a significant fraction of a wavelength Even short lengths of wiring add serious parasitics
Transmission-line losses are high low Q in VCO resonators and filters high combining losses in PAs: low power, low efficiency several dB added noise in LNAs.

## Slide 43: Thin-film microstrip: inverted or right-side-up

## Slide 44: 130nm /1.1 THz InP HBT ICs to 670 GHz
614 GHz fundamental VCO
340 GHz dynamic frequency divider
620 GHz, 20 dB gain amplifier
M Seo, TSC IMS 2013
also: 670GHz amplifier J. Hacker , TSC IMS 2013 (not shown)
M. Seo, TSC / UCSB
M. Seo, UCSB/TSC IMS 2010
204 GHz static frequency divider (ECL master-slave latch)
Z. Griffith, TSC / UCSB CSIC 2010
300 GHz fundamental PLL
M. Seo, TSC IMS 2011
220 GHz 180 mW power amplifier
T. Reed, UCSB CSICS 2013
600 GHz Integrated Transmitter PLL + Mixer
M. Seo TSC
Integrated 300/350GHz Receivers: LNA/Mixer/VCO
M. Seo TSC
81 GHz 470 mW power amplifier
H-C Park UCSB IMS 2014

## Slide 45: 214 GHz, 180mW Power Amplifier (330 mW design)
2.3 mm x 2.5 mm
T. Reed, Z. Griffith, 2014 CSICS http://ieeexplore.ieee.org/xpls/abs_all.jsp?arnumber=6659187&tag=1

## Slide 46: 205GHz Logic in Thin-Film Inverted Microstrip
8:1, 205 GHz static divider in 256 nm InP HBT. Image taken before top metal (ground plane) deposition
205 GHz divider, Griffith et al, IEEE CSICS, Oct. 2010

## Slide 47: 140GHz Transceivers: GF 22nm SOI CMOS
1.9 mm
0.76 mm
1.9 mm
0.76 mm
A. Farid UCSB, 2019 RFIC symposium

## Slide 48: RX Characterization

## Slide 49: TX Characterization

## Slide 50: InP Power Amplifier Design
Class-A mm-Wave Power Amplifiers 120, 140, 220, 300GHz designs Power: 50-100-200mW 140GHz efficiencies: 17%
Class-B mm-Wave Power Amplifiers 120GHz designs Power: 30 mW 140GHz efficiencies: 28%
ICs taped out Feb. 2019 Presently in fabrication Expected test: late summer
James Buckwalter, Mark Rodwell: UCSB
# | Description | Area(mmmm)
1 | 140GHz,Pout=19.3dBm, PAE=13%, Gain=23.2dB | 0.631.08
2 | 140GHz, Pout=21.8dBm, PAE=13.5%, Gain=23.4dB | 1.2 1.09
3 | 140GHz,Pout=19.8dBm, PAE=6.6%, Gain=24.8dB | 0.951.07
4 | 140GHz,Pout=19.5dBm, PAE=17.9%, Gain=14.5dB | 0.63
5 | 220GHz,Pout=20.2dBm, PAE=7.8%, Gain=19.7dB | 1.090.78
6 | 140GHz,Pout=19.3dBm, PAE=17.1%, Gain=14.4dB | 0.60.79
7 | 220GHz,Pout=15.9dBm, PAE=10.2%, Gain=17.9dB | 0.560.79
8 | 300GHz,Pout=13.5dBm, PAE=4.2%, Gain=13.5dB | 0.630.8
9 | 300GHz,Pout=17.8dBm, PAE=3.5%, Gain=15.8dB | 1.10.94
10 | 140GHz,Pout=19.7dBm, PAE=8.1%, Gain=17.7dB | 0.950.9
11 | 140GHz,Pout=21.7dBm, PAE=10.4%, Gain=30.7dB | 1.21.3
12 | 120GHz, Pout=20.4dBm, PAE=9.2%, Gain=20.4dB | 0.950.98
13 | 140GHz, Pout=17.3dBm, PAE=7.5%, Gain=25.3dB | 1.070.54
14 | 140GHz, Pout=15dBm, PAE=28%, Gain=16dB | 
# | Description | 
1 | 140GHz,Pout=19.3dBm, PAE=13%, Gain=23.2dB | 
2 | 140GHz, Pout=21.8dBm, PAE=13.5%, Gain=23.4dB | 
3 | 140GHz,Pout=19.8dBm, PAE=6.6%, Gain=24.8dB | 
4 | 140GHz,Pout=19.5dBm, PAE=17.9%, Gain=14.5dB | 
5 | 220GHz,Pout=20.2dBm, PAE=7.8%, Gain=19.7dB | 
6 | 140GHz,Pout=19.3dBm, PAE=17.1%, Gain=14.4dB | 
7 | 220GHz,Pout=15.9dBm, PAE=10.2%, Gain=17.9dB | 
8 | 300GHz,Pout=13.5dBm, PAE=4.2%, Gain=13.5dB | 
9 | 300GHz,Pout=17.8dBm, PAE=3.5%, Gain=15.8dB | 
10 | 140GHz,Pout=19.7dBm, PAE=8.1%, Gain=17.7dB | 
11 | 140GHz,Pout=21.7dBm, PAE=10.4%, Gain=30.7dB | 
12 | 120GHz, Pout=20.4dBm, PAE=9.2%, Gain=20.4dB | 
13 | 140GHz, Pout=17.3dBm, PAE=7.5%, Gain=25.3dB | 
14 | 140GHz, Pout=15dBm, PAE=28%, Gain=16dB | 

## Slide 51: 140GHz PA: power and S-parameter simulations
Technology | 250-nm InP HBT
Freq, GHz | 140
VCC, V | 2.5
Jbias,mA/um | 1.3
S21, dB | 25
Pout ,dBm, 2dB | 19.1
PAE % , 2dB | 12.6
Psat ,dBm | 20.9
PAEsat % | 18.3
BW3dB, GHz | 43
PDC, W | 0.65

## Slide 52: 220GHz PA (CB version)
Technology | 250-nm InP HBT
Freq, GHz | 220
VCC, V | 2.8
Jbias,mA/um | 1.3
S21, dB | 22.3
Pout ,dBm, 2dB | 21
PAE % , 2dB | 8.3
Psat ,dBm | 22
PAEsat % | 10.4
BW3dB, GHz | 48
PDC, W | 1.5
Power cell: Smaller base capacitor, SRF=679GHz Decrease the shunt inductor
Two stage drivers: Similar to power cell with higher cap SRF=512GHz
Area=1.09 mm × 0.78mm

## Slide 53: 300GHz PA (CB version)
Technology | 250-nm InP HBT
Freq, GHz | 300
VCC, V | 2.5
Jbias,mA/um | 1.3
S21, dB | 17.6
Pout ,dBm, 2dB | 17.8
PAE % , 2dB | 3.5
Psat ,dBm | 19.4
PAEsat % | 5
BW3dB, GHz | 43
PDC, W | 1.65
power cell and driver:
Decrease base cap and inductor
SRF=714GHz
Three driver stages
Area=1.1 mm × 0.94mm
Four fingers, LE =6um.

## Slide 54
Packages

## Slide 55: The mm-wave module design problem
How to make the IC electronics fit ? 100+ GHz arrays: l0/2 element spacing is very small. Antennas on or above IC → IC channel spacing = antenna spacing → limited IC area to place circuits
How to avoid catastrophic signal distribution losses ? long-range, high-gain arrays: array size can be large. ICs beside array → very long wires between beam former and antenna → potential for very high signal distribution losses
How to remove the heat ? 100+ GHz arrays: element spacing is very small. If antenna spacing = IC channel spacing, then power density is very large

## Slide 56: mm-wave/sub-mm-wave packaging
Not all systems steer in two planes... ...some steer in only one.
Not all systems steer over 180 degrees... ...some steer a smaller angular range
Arrays can often be linear (1D), instead of rectangular (2D) Element spacing can often be greater than l/2.
→ Array packaging then greatly simplified.

## Slide 57: Concept: Tile for linear arrays
Terrestrial system: horizontal steering only→ linear array. Space at edges of linear array: room for III-V PAs, LNAs. Alternating-sides feed: 2mm pitch→ room for large GaN PAs. Mounting directly on metal carrier→ heatsinking.

## Slide 58: 140GHz array module design
-1.4 dB
-0.53 dB
Simulations good: working with Kyocera. June tapeout ?

## Slide 59: 140GHz Indoor Gigabit Network Demonstration

## Slide 60: Concept: module for small angular scanning
Terrestrial system: horizontal + vertical steering → rectangular array. Limited angular steering range (installation)→ spacing >> l/2 Endfire / edge-card geometry: room for III-V PAs, LNAs. Mounting directly on metal carrier→ heatsinking.
If Vivaldi's are replaced with dipoles, element spacing can be reduced to l/2. → potential for wider angular scanning

## Slide 61: l/2-spaced 2-D Arrays
Tray design Vertical spacings become very small difficult to remove heat
Split-block / waveguide design heatsinking maintained difficult to manufacture

## Slide 62
Wireless above 100GHz

## Slide 63: Wireless above 100 GHz
Massive capacities large available bandwidths massive spatial multiplexing in base stations and point-point links
Very short range: few 100 meters short wavelength, high atmospheric losses. Easily-blocked beams.
IC Technology All-silicon for short ranges below 250 GHz. III-V LNAs and PAs for longer-range links. Just like cell phones today III-V frequency extenders for 340GHz and beyond
The challenges spatial multiplexing: computational complexity packaging: fitting signal channels in very small areas

## Slide 64
In case of questions

## Slide 65: 140 GHz spatially multiplexed base station

## Slide 66: 75 GHz spatially multiplexed base station
If we use instead a 75GHz carrier, the range increases to 325 meters (vs. 250 meters) but the handset becomes 16mm×16mm (vs. 9mm×9mm), and the hub array becomes 9mm×655mm (vs. 5mm×350mm)
Or, use a 4×4 (8mm×8mm) handset array, and the range becomes 210 meters.

## Slide 67: 340 GHz 640 Gb/s MIMO backhaul

## Slide 68: 340 GHz 5 Tb/s MIMO backhaul
requires 10mW output per element ...10W total radiated power