## Slide 1: Transistors for 100-300GHz Wireless
Mark Rodwell, Brian Markman, Yihao Fang, Logan Whitaker, Hsin-Ying Tseng, A. S. H. Ahmed University of California, Santa Barbara rodwell@ece.ucsb.edu
This work was supported in part by the Semiconductor Research Corporation (SRC) and DARPA
Plenary, ESSCIRC ESSDERC 2021 European Solid-state Circuits and Devices Conference, Grenoble and online. September 15, 2021.

## Slide 2: Acknowledgements
Also: Kyocera: D. Kim, H. Horikawa, M. Imayoshi. Samsung: G. Xu, N. Sharma, S. Abu-Surra, W. Choi Pi-Radio: A. Dhananjay,

## Slide 3: Transistors for 100-300GHz wireless
100-300GHz carriers, massive spatial multiplexing → Terabit hubs and backhaul links, high-resolution imaging radar
Wireless networks: exploding demand.
Immediate industry response: 5G. ~6~100GHz increased spectrum, extensive beamforming
Next generation: 100-300GHz (???) greatly increased spectrum, massive spatial multiplexing
What transistors do we need ?

## Slide 4: 140GHz, 160 Gb/s MIMO network hub
Hub with 32-element array (four 1×8 modules): 16 users/array. F=8dB LNAs, P1dB=21 dBm PAs 10 Gb/s/beam→ 160 Gb/s total capacity 40 m range in 50mm/hr rain with 17dB total margins
Handset: 8 × 8 array (9×9mm)

## Slide 5: 8-channel 140GHz MIMO hub modules
110mW power amplifier Teledyne 250nm InP HBT 20.8% PAE
Transmitter IC GlobalFoundries 22nm SOI CMOS
A. Farid et. al, in review
Kyocera LTCC carrier

## Slide 6: 210 GHz, 640 Gb/s MIMO backhaul
8-element MIMO array 3.1 m baseline for 500 meters range. 80Gb/s/subarray→ 640Gb/s total 4 × 4 sub-arrays → 8 degree beamsteering
Key link parameters 500 meters range in 50 mm/hr rain; 23 dB/km 20 dB total margins: packaging loss, obstruction, operating, design, aging LNAs: 6dB noise figure PAs: 18dBm =P1dB (per element)

## Slide 7: 210 GHz transmitter and receiver ICs
210GHz transmitter: 20GHz bandwidth, 15.5-16.5dBm power
Size: 2.3 x 0.85 mm2
Size: 2.9 x 0.75 mm2
M. Seo et al, 2021 IMS; Teledyne 250nm InP HBT
210GHz receiver: 20GHz bandwidth, 7.7-9.5dB noise figure
280GHz transmitter: 17dBm power (simulated)
280GHz receiver: 11dB noise figure, 40GHz bandwidth (sim.)
Solyu, Alz, Ahmed, Seo; UCSB/Sungkyunkwan; Teledyne 250nm InP HBT

## Slide 8: 100-300GHz wireless: transistor requirements
Transmitters need: high power-added efficiency high added power density (Pout-Pin)/(gate width, emitter length) Receivers need: low cascaded noise
Need reasonable gain/stage. die area, power, accumulated gain compression
(gain in PAs, LNAs is less than MAG/MSG, U, ... )

## Slide 9: Transistors for 100-300GHz
CMOS: good power & noise up to ~150GHz. Not much beyond. 65-32nm nodes are best.
InP HBT: record 100-300GHz PAs
SiGe HBT: outperforms CMOS above 200GHz
GaN HEMT: record power below 100GHz. Bandwidth improving
InGaAs-channel HEMT: world's best low-noise amplifiers
*results with low PAE at high Psat or low Psat with high PAE are not shown
Results compiled 8/1/2021

## Slide 10: Where the IC designer can't help us.
mm-wave transistor gain is low: gain-boosting is common Common-source vs. common-gate. Capacitive neutralization. Controlled positive feedback (Singhakowinta, Int. J. Electronics, 1966) Such circuits don't improve the parameters that matter the most. The circuit* doesn't change the transistor minimum cascaded noise figure. (Haus, Adler, Proc. IRE, 1958) The circuit* doesn't change the transistor maximum efficiency vs. added power curve.
*If lossless, and given the correct source and load impedances.

## Slide 11: Current density, finger pitch limit cell output power

## Slide 12: Current density, finger pitch limit cell output power
High Vbr, low Imax ? Device sized to drive 50W might approach lg/4 width. Small finger pitch is critical; limited by thermal design
50W GaN PA cell @ 140GHz (1.6W) 25V swing, 1.67mA/mm, gates: 30 mm width, 15 mm pitch
50W InP HBT PA cell @ 280GHz (40mW) 4V swing, 3.3mA/mm, emitters: 6 mm length, 6 mm pitch
K. Shinohara, Teledyne: GaN HEMT thermal analysis

## Slide 13: Current density, finger pitch limit power combining
More cells: more output power
Number of cells limited by combining losses.
Losses mostly limited by size.
Can 50W cell fit in lg/8 (120 mm) pitch ? →8:1 combining with 0.4dB loss @200GHz
Can 50W cell fit in lg/24 (40 mm) pitch ? →16:1 combining with 0.5dB loss @200GHz
200GHz InP HBT PA: 80 mm cell pitch

## Slide 14: mm-Wave Transistor Development
THz InP HBTs: State-of-art: 1.1THz fmax @ 130nm node (Teledyne: Urteaga, DRC 2011) Efficient 100-650GHz power
THz InP HEMTs: State-of-art: 1.5THz fmax @ 32nm node (NGST: X. Mei, EDL 2015) Sensitive 100-650GHz low-noise amplifiers high-K gate dielectric *might* permit further scaling.
InGaN and GaN HEMTs: Leading power technology to ~110GHz Efforts to extend this to 140, 220GHz.
N-polar GaN: Mishra, UCSB
Rode , IEEE TED 2015

## Slide 15: Transistor scaling laws: ( V,I,R,C,t ) vs. geometry
Bulk and Contact Resistances
Depletion Layers
Thermal Resistance
Fringing Capacitances
Available quantum states to carry current
→ capacitance, transconductance contact resistance

## Slide 16: Degenerate State Density (Ballistic) Limits

## Slide 17: Bipolar Transistor Design: Scaling

## Slide 18: Bipolar Transistor Scaling Laws
Narrow junctions. Thin layers High current density Ultra low resistivity contacts

## Slide 19: Refractory Ohmic Contacts to In(Ga)As
Refractory: robust under high-current operation / Low penetration depth: ~ 1 nm
32 nm (2.8THz) node requirements
Baraskar et al, Journal of Applied Physics, 2013
Why no ~2THz HBTs today? Problem: reproducing these base contacts in full HBT process flow

## Slide 20
InP HBTs: 1.07 THz @200nm, ?? @ 130nm
?
Rode et al., IEEE TED, Aug. 2015
Rode , IEEE TED, Aug. 2015

## Slide 21: THz Transistor Measurements
Simple pads: Substrate coupling: need small pads, narrow CPW Ambiguity in pad stripping order. UCSB 130nm HBTs: order not important. Add through & load to remove ambiguity
On-wafer through-reflect-line: No ambiguity from pad stripping. Calibration to line Zo Still must avoid substrate mode coupling CPW particularly vulnerable. better: thin-film microstrip or ~25 mm substrate with TSV's
D. F. Williams, A. Young, M. Urteaga, "A Prescription for Sub-Millimeter-Wave Transistor Characterization," IEEE Transactions on Terahertz Science and Technology, July 2013
Rodwell, IEDM 2017
Urteaga, DRC 2011

## Slide 22: Challenges @ 64nm/2THz, 32nm/3THz Nodes
Baraskar et al, Journal of Applied Physics, 2013
Need high base contact doping >1020/cm3 for good contacts high Auger recombination very low b.
Seem to need 1-3nm contact penetration Pd or Pt contacts react with 3++ nm of base penetrate surface contaminants too deep for thin base
Base regrowth as possible solution thin, moderately-doped intrinsic base InGaAs or GaAsSb @ 1019-1020/cm3 thick, heavily-doped extrinsic base P-GaAs, ~1021/cm3
Rode et al., IEEE TED, Aug. 2015

## Slide 23: Regrown-Base InP HBTs: Images
Cross-sections
Dry-etched TiW emitter contact

## Slide 24: Regrown-Base InP HBTs: Status
Excellent base contacts; but hydrogen base passivation 0.4 W-mm2 resistivity for GaAs/metal contact 290 W sheet resistivity for regrown base  0.60W-mm2 resistivity for InGaAs/GaAs contact✘ 1940W/ sheet resistivity for intrinsic base ✘
Good DC data: even given regrowth refractory Mo/W/TiW emitter contact maintains low rc.
Recent efforts: in-situ MOCVD hydrogen anneal Preliminary results: marginal ~300GHz fmax (still excessive hydrogen)

## Slide 25: FETs (HEMTs): key for low noise
2:1 to 4:1 increase in ft : improved noise less required transmit power smaller PAs, less DC power
or higher-frequency systems

## Slide 26: High-Frequency FET Scaling
To double ft , reduce Lg 2:1, but this is not enough
Must also reduce Cgsx/gm , Cgd/gm time constants 2:1
→ gm/Wg must be doubled
Must also thin dielectric and channel by 2:1 (gmRds)

## Slide 27: FET Current and Transconductance
To increase gm: thin the oxide & channel and increase K1 (mass, # valleys)…hard or increase (Vgs-Vth)…also hard

## Slide 28
Towards faster HEMTs: InAs MOS-HEMTs
Thinner gate insulator HEMT: ~6nm InAlAs (er=12), limited by tunneling MOS-HEMT: 2nm ZrO2 (er=25)
Less source resistance HEMT: InAlAs barrier under N+ source/drain MOS-HEMT: N+ layer on InAs channel
1st MOS-HEMT demonstration: Fraunhofer IAF / IBM Zurich
Simple ballistic theory: thin dielectric→ increased gm. HEMT: InAlAs barrier: tunneling, thermionic leakage
Limitations to theory: Assumes parabolic E-k dispersion: unrealistic Ignores effect of maximum gate overdrive (Vgs-Vth)

## Slide 29: MOS-HEMT: fabrication flow

## Slide 30: MOS-HEMT: device structure
tch | Channel Material | ZrO2 Cycles
7.0 nm | InAs / InGaAs | 30
B. Markman et. al, 2021 DRC

## Slide 31: DC characteristics @ 40 nm Lg , 2 × 10µm Wg
Peak gm | RA | Ion | Ioff | Ig | Long Lg SSmin
2.4 mS/µm | 49 – 55 Ω•µm | > 1.45 mA/µm | < 10 nA/µm | < 10 nA/µm | 76 mV/dec
B. Markman et. al, 2021 DRC

## Slide 32: RF characteristics @ 40 nm Lg , 2 × 10µm Wg
VDS = 0.70 V VGS = 0.30 V IDS = 0.79 mA/µm
fꚍ = 420 GHz fmax = 562 GHz
Peak fꚍ = 420 GHz on Lg = 40 nm conduction device, peak fmax at Lg = 50 nm
fmax extrapolation difficult because of peaks in U; calibration artifacts or negative resistance

## Slide 33: Need for higher energy barriers
To increase transconductance: thin the oxide, thin the well → increased eigenstate energy → loss of confinement at large (Vgs-Vth) → constrains maximum transconductance: ID∝(Vgs-Vth)3/2 → gm∝(Vgs-Vth)1/2 → maximum achievable gm.
Need high barrier energies InAs/InAlAs vs InAs/AlAsSb InP/AlAsSb ????
Huang, JAP, 2014
B. Markman

## Slide 34: Transistors for 100-300GHz wireless
Systems Multi-beam (MIMO) endpoint and backhaul links. Imaging radar
Transistor parameters LNAs: cascaded noise figure PAs: high PAE, high power density (W/mm) high ft × Vbr PAs need high A/mm & closely-spaced fingers
Today's available IC technologies CMOS: good to ~150GHz. 65-32nm nodes are best. SiGe: surpasses CMOS above 200GHz. InP HBT: record 100-300GHz PAs GaN HEMT: record power below 100GHz. Improving InGaAs FETs: record LNAs
Improved InP HBTs goal: improved PAE in 100-300GHz PAs. challenge: base contact resistivity scaling. Process complexity.
Improved InGaAs FETs High-K gate dielectric may permit further scaling. High-K / InP / AlAsSb ?

## Slide 35
In case of questions

## Slide 36: 210 GHz FMCW crossed-array imaging car radar
Array: 36×1 transmit, 1×216 receive 36 (v) × 216 (h) image length: 15cm (6 inches), beamwidth: 0.27o, view: 10o (v) ×90o (h). scan: 40Hz
Electronics transmit power/element: 50mW receiver noise: 6dB packaging losses: 2dB TX, 2dB RX
Sees: 22cm diameter target (a soccer ball) @ -10dB reflectivity 200m range, with 10dB SNR in heavy fog/rain @ 22dB/km with 4dB operating margins.

## Slide 37: FET Scaling Laws (these now broken)
FET parameter | change
gate length | decrease 2:1
current density (mA/mm) | increase 2:1
specific transconductance (mS/mm) | increase 2:1
transport mass | constant
2DEG electron density | increase 2:1
gate-channel capacitance density | increase 2:1
dielectric equivalent thickness | decrease 2:1
channel thickness | decrease 2:1
either (channel state density) | increase 2:1
or (Vgs-Vth) | increase 4:1
contact resistivities | decrease 4:1
Gate dielectric can't be much further scaled. Not in CMOS VLSI, not in mm-wave HEMTs
gm/Wg (mS/mm) hard to increase→ Cend / gm prevents ft scaling.
Shorter gate lengths degrade electrostatics→ reduced gm /Gds → reduced fmax , ft