## Slide 1
(Paper x.x)
135GHz CMOS / LTCC MIMO Receiver Array Tile Modules
  Ali A. Farid1,2, Ahmed S. H. Ahmed1,3, Aditya Dhnanjay4,
  Mark J. W. Rodwell1
1University of California, Santa Barbara, USA
2Intel Corporation, USA
3Marki Microwave, USA
4Tandon school of Engineering, NYU, USA
Notes: The slide guide is meant to be used with PowerPoint.

## Slide 2: Outline
Motivation
IC-Package Interconnect technology
Interposer Stack build up
Integrated Receiver module
Module Wireless Link Experiment
Conclusion

## Slide 3: Opportunities and challenges at mmwave
Large available spectrum ()
Massive # of parallel channels, Multiple independent beams
Low-cost high-performance packaging (?)
A. Farid at al, RWS2021

## Slide 4: IC and Package Interconnect
A. Farid at al, RFIC2019
Direct Conversion RX in GF-22FDSOI
20GHz 3-dB BW
27dB Conversion gain
Mark Rodwell, "100-300GHz Wireless: Transistors, ICs, packages, systems.“6G Workshop, IEEE RF/Wireless Week (RWW2021), 17 - 20 January San Diego, California, USA
Type | Transition Loss/ Frequency | Technology | Cost | Heatsinking | 
(ball) wirebonds | 100 GHz ✘ | Industry standard | low | good | 
ribbon, mesh bond | 200 GHz | Handcrafted | high ✘ | good | 
patch antennas on superstrate | 1000 GHz | Straightforward | low | good | 
Cu stud flip-chip | >200 GHz | Industry standard | low | OK | 

## Slide 5: IC and Package Interconnect
A. Farid at al, RFIC2019
Chip bonded to LTCC carrier using 50μm diameter copper pillar
Pillars equally spaced at 125μm
IC-package transition loss of 1dB
A. Farid at al, BCICST2021

## Slide 6: MIMO 1-D Array Tile
Ceramic Interposer
Lower Cost PCB!
High Lithographic resolution (40μm) | 
0.6λ antenna spacing | 
Dense wirebond routing from Interposer to carrier board | 
Higher Cost and slower turnaround time | 
Coarse Lithographic resolution (80μm) | 
λ antenna spacing | 
No need for wire bonding (all solution on one board) | 
Lower Cost? | 

## Slide 7: Challenges with the PCB approach
Issues | Lessons learned
Difficulty in bonding copper studs to PCB Over etched boards/poor quality Wider solder mask opening Thick solder mask layers | PCB unsuitable for copper pillars High resolution PCB is expensive

## Slide 8: Integrated Receiver Module on LTCC
4 channels/side
8-elements series fed-patch antenna/channel
0.65λ antenna spacing
I/Q , LO, DC signals routed from LTCC to PCB using AL wirebonds (1.25mil)

## Slide 9: Module Calibration and Testing Setup
Rx module connected to ZCU-111 for array calibration and beamforming.
Test transmitter mounted at 15cm distance on a rotating arm.
Wideband 1-GHz OFDM signal used for array calibration (explain briefly)
https://github.com/pi-radio/Pi-Radio-v1-NRT
https://dl.acm.org/doi/abs/10.1145/3411276.3412195

## Slide 10: Module Conversion Gain & Radiation Pattern
8-working channel
floating ground!
4-working channel
1.3 λ antenna spacing (Limited F.O.V)

## Slide 11: Receiver Module Wireless Link
In single-beam operation: there is –
13.5dB RMS EVM in 1.34Gb/s QPSK
13dB EVM, RMS in 1.92Gb/s 16QAM
What is limiting Module datarate?

## Slide 12: Comparison with state of the art
 | Townley CICC2020 | Singh RFIC2020 | S. Li IMS2021 | Abu-Surra ICC2021 | Sawaby RFIC2020 | This Work
Freq (GHz) | 113 | 115-155 135-170 | 140 | 140 | 135 | 135
IC Technology | 28nm CMOS | 0.13μm SiGe | 45nm SOI | 45nm SOI | 0.13μm SiGe | 22FD-SOI
Package Technology | PCB | Radio on Glass | Quartz Superstrate | PCB | PCB + Lens | LTCC Interposer
Type | 1 Channel | 1 Channel | Single beam | MIMO$ | 2x2 LOS MIMO | MIMO
# of channels | 2 | 1 | 8 | 4,8, and 16 | 2 | 8
Antenna | Yes | No | Yes | Yes | Yes | Yes
Data rate | 80Gb/s | 36Gb/s 8Gb/s | 16Gb/s 18Gb/s | 6Gb/s | 2x16Gb/s | 3Gb/s
Format | 16QAM | 64QAM /256QAM | QPSK 64QAM | 16QAM | QPSK | 16QAM
EVM | -- | -23dB -30dB | 6.25% 5.5% | NA | -- | -13.5dB -13dB
Link | Air | WR-6 | Air | Air | Air | Air
Distance | 10cm | -- | -- | 15m | 6cm | 15cm

## Slide 13: Conclusion
Packaging approach for massive MIMO arrays in Tile
Assembly challenges with advanced copper pillars
Why PCB approach is not the right candidate
Tile of 8-elements with 3Gb/s per beam

## Slide 14: Acknowledgment
Authors would like to thanks
Kyocera Japan for ceramic interposer fabrication
Kyocera San Diego for module assembly
GlobalFoundries for CMOS chip fabrication and free access to advanced copper pillars
This work was supported in part by the Semiconductor Research Corporation and DARPA under the JUMP program.

## Slide 15
Questions?