## Slide 1: Lg = 40nm Composite Channel MOS-HEMT Exhibiting fτ = 420 GHz, fmax = 562 GHz
Brian Markman, Simoné Tommaso Šuran Brunelli, Matt Guidry, Logan Whitaker, and Mark Rodwell
UCSB Department of Electrical and Computer Engineering
Funding: SRC & DARPA

## Slide 2
High fτ , fmax HEMT Motivation
MOS-HEMT Advantage
Device 1 – Link Wet Etched
  Fabrication
  DC Characteristics
  RF Characteristics
Device 2 – Link “Recessed”
  Fabrication
  DC Characteristics
  RF Characteristics

## Slide 3: High fτ , fmax HEMT Motivation
Current electromagnetic bands are crowded
Need to move into currently unallocated bands at higher frequencies
Higher frequency = higher data rate = faster upload/download speeds
For circuits to be efficient (high PAE) need fop ≈ 0.1-0.2 • fmax
Atmospheric attenuation means many base stations and spatial multiplexing

## Slide 4: HEMT Motivation – Reduce Noise Figure
2:1 to 4:1 increase in ft :
  Improved noise
  Less required transmit power
  Smaller PAs, less DC power
Or higher-frequency systems
Reprinted with permission of Mark Rodwell

## Slide 5: Noise Figure / Measure Considerations
Signal out
LNA
PA 1
PA 2
PA 3
PA = Power Amplifier
LNA = Low Noise Amplifier
Noise of cascaded amplifiers is more important than noise of one
F∞ can be big even if F1 is small  cannot forget G1
Cannot forget about fmax  Need balanced fꚍ , fmax
Signal in

## Slide 6: Reduce Noise Figure – What Device?
MOSFETs
Gate dielectric and Lg can't be much further scaled (CMOS and mm-wave)
gm/Wg (mS/mm) hard to increase → Cend / gm prevents ft scaling
Move source-drain further away  HEMTs

## Slide 7
Reduce Noise Figure – What Device?
MOSFETs
Gate dielectric and Lg can't be much further scaled (CMOS and mm-wave)
gm/Wg (mS/mm) hard to increase → Cend / gm prevents ft scaling
Move source-drain further away  HEMTs
HEMTs
Gate leakage current density  small CBO of InAlAs to InGaAs
RS associated with getting electrons through widegap modulation doped link

## Slide 8: Reduce Noise Figure – What Device?
MOSFETs
Gate dielectric and Lg can't be much further scaled (CMOS and mm-wave)
gm/Wg (mS/mm) hard to increase → Cend / gm prevents ft scaling
Move source-drain further away  HEMTs
HEMTs
Gate leakage current density  small CBO of InAlAs to InGaAs
RS associated with getting electrons through widegap modulation doped link
MOS-HEMTs
Replace InAlAs gate dielectric with high-k
  Reduces gate leakage, increases Cg-ch, increases gm, increases ft
  Better electrostatics, increases gm / GDS, increases fmax
Regrowth process rather than recess etch process
  Place N+ source-drain directly on channel, reduces RS, increase gm

## Slide 9: Device 1 – Link Wet Etched

## Slide 10: Device 1 – Device Structure
InAlAs
InP etch stop
InAlAs
N+ InGaAs
Ni
Au
Au
Ni
InAlAs
Composite link
Channel
InP
Ni
Au
Undercutting
InAlAs
Ni
High-k
AlxOyNz
~17.5nm
tch | Channel Material | ZrO2 Cycles
2.5 nm | InGaAs | 30

## Slide 11: Device 1 – DC Characteristics
Peak gm | RA | Ion | Ioff | Ig | Long Lg SSmin
1.6 mS/µm | 69 Ω•µm | > 0.75 mA/µm | > 1.0 µA/µm | < 10 nA/µm | N/A
Same as [1]  likely large Rend due to isotropic undercut, Rvert likely lower

## Slide 12: Device 1 – Peak Performance
Peak fꚍ = 356 GHz and fmax = 403 GHz on the same device (Lg = 12 nm conduction)
Shift to larger VGS due to thin channel and higher VDS
Why aren’t gm and ft larger? Channel is thin, have high-k, both should be high!

## Slide 13
Thin channel gives large CQW and CDOS
  CQW: Wave-function moves towards oxide
  CDOS: in-plane effective mass increases
Thin Channels are not the Whole Picture
Fermi Level moves to populate low DOS
Oxide
Channel
Back Barrier
Wave function has “thickness”
Oxide
Channel
Back Barrier

## Slide 14
Thin channel gives large CQW and CDOS
  CQW: Wave-function moves towards oxide
  CDOS: in-plane effective mass increases
Thin Channels are not the Whole Picture
Fermi Level moves to populate low DOS
Oxide
Channel
Back Barrier
Wave function has “thickness”
Oxide
Channel
Back Barrier

## Slide 15: Ultra-thin Body Quantum Wells
Maximum , depends on band offset of channel | back barrier
Thin Channel Take-Aways:
  Larger  less available , small m* channels  E1 move faster
  Channel needs to be thick enough for small E1 = high gm,i, IDS
  Channel needs to be thin enough for high Cgs,i and high aspect ratio (gm / GDS)
  Sweet spot ~6-10nm, unsurprisingly consistent with SOA MOSFETs and HEMTs

## Slide 16: Device 1 – Take Away
Wet etching gives unpredictable link region profile
RS moderately reduced but isotropic profile not worth reduction
  Results in larger RL due to resistive ends
Thin channels limit maximum gm
Low Ig  room to thin high-k
Optimize channel thickness  thicker NOT thinner

## Slide 17: Device 2 - Fabrication

## Slide 18: Device 2 – Device Structure
tch | Channel Material | ZrO2 Cycles
7.0 nm | InAs / InGaAs | 30

## Slide 19: Device 2 – DC Characteristics
Peak gm | RA | Ion | Ioff | Ig | Long Lg SSmin
2.4 mS/µm | 49 – 55 Ω•µm | > 1.45 mA/µm | < 10 nA/µm | < 10 nA/µm | 76 mV/dec

## Slide 20: Device 2 – Peak Performance – Lg = 40 nm, Wmesa = 10µm
VDS = 0.70 V
VGS = 0.30 V
IDS = 0.793 mA/µm
fꚍ = 420 GHz
fmax = 562 GHz
Peak fꚍ = 420 GHz on Lg = 40 nm conduction device, peak fmax at Lg = 50 nm
Extrapolation of fmax difficult because of noisy U  occasionally see “spiking”

## Slide 21: Deice 2 – Take Away
Link thinning gives excellent RS and predictable profile
Peak gm likely limited source-starvation  need more nLink
Low Ig  room to thin high-k
Need to improve T-Gate process to reduce CGS,p and CGD,p

## Slide 22: HEMT / MOS-HEMT State-of-the-Art
UCSB 2018 – 2021
Tokyo 2013
Fraunhofer 2019
Teledyne 2011
NTT 2018 – 2019
NGC 2015
HEMTs
MOS-HEMTs

## Slide 23: Conclusions
Extremely high gm = 2.9 mS/µm  competitive with SOA HEMTs
Extremely low RS < 100 Ω•µm  will increase with InAlAs link
Extremely low gds = 0.2 mS/µm  significantly better than SOA HEMTs
Improving high frequency FOMs  fꚍ , fmax > 400 GHz
Need to improve T-Gate process to reduce parasitics!

## Slide 24: MOS-HEMT Future Work
Problems:
Peak fꚍ severely limited by large CGS,p  need a self-aligned process
Peak fmax limited by large RG (poor yield & reproducibility)  improve T-Gate process
Low breakdown voltage and therefore low power-handling  wide Eg channel
Solutions:
Self-Aligned “Regrowth Reversal” Process  reduces CGS,p and improves T-Gate process
Wide-bandgap back-barriers (AlAsSb) for improved GDS
InP channel / AlAsSb back-barrier MOS-HEMT for high-power

## Slide 25: Acknowledgements
Funding: DARPA ComSenTer

## Slide 26: QUESTIONS

## Slide 27
FET parameter | change
gate length | decrease 2:1
current density (mA/mm) | increase 2:1
specific transconductance (mS/mm) | increase 2:1
transport mass | constant
2DEG electron density | increase 2:1
gate-channel capacitance density | increase 2:1
dielectric equivalent thickness | decrease 2:1
channel thickness | decrease 2:1
channel state density | increase 2:1
contact resistivities | decrease 4:1
FET Scaling Laws (Now Broken)
Fermi Level moves to populate low DOS
Oxide
Channel
Back Barrier
Wave function has “thickness”
Oxide
Channel
Back Barrier

## Slide 28
S21/5
S11
5•S12
S22
[1] Device 0 SSEC: Lg = 8 nm

## Slide 29: Device 1 SSEC: Lg = 12 nm
VDS = 1.00 V
VGS = 0.50 V
IDS = 0.664 mA/µm
fꚍ = 375 GHz
fmax = 326 GHz
S21/5
S11
5•S12
S22
SSEC very difficult to fit… do not trust this model

## Slide 30: Device 2 SSEC: Lg = 40 nm
Significantly improved fit, trustable

## Slide 31: Model vs. Extrapolation
Device | Extraction | Lg (nm) | fꚍ (GHz) | fmax (GHz)
0 | Extrapolation | 8 | 511 | 256
0 | Modeled | 8 | 533 | 204
1 | Extrapolation | 12 | 356 | 398
1 | Modeled | 12 | 375 | 326
2 | Extrapolation | 40 | 402 | 560
2 | Modeled | 40 | 454 | 567

## Slide 32: [1] Device 0 - Fabrication

## Slide 33: [1] Device 0 – Device Structure
tch | Channel Material | ZrO2 Cycles
6.5 nm | InAs / InGaAs | 40

## Slide 34: [1] Device 0 – DC Characteristics
Peak gm | RA | Ion | Ioff | Ig | Long Lg SSmin
2.2 mS/µm | 68 – 85 Ω•µm | > 0.90 mA/µm | > 1.0 µA/µm | < 10 pA/µm | N/A

## Slide 35: [1] Device 0 – Peak Performance

## Slide 36: Device 1 – RF Characteristics
Rapid drop in FOMs due to thin channel
Balanced fꚍ , fmax
Low peak gm,e ≈ 2.0 mS/µm
Excellent gds,e ≈ 0.3 mS/µm
Extremely high CGS ≈ 0.9 fF/µm
High CGD ≈ 0.3 fF/µm
Improved RG ≤ 10 Ω

## Slide 37: Device 2 – RF Characteristics
Gradually decreasing fꚍ
Constant / increasing fmax
Balanced fꚍ , fmax
Maintained RG ≤ 10 Ω
Extremely high CGS ≈ 0.9 fF/µm
High CGD ≈ 0.4 fF/µm
High peak gm,e ≈ 2.9 mS/µm
Excellent gds,e ≈ 0.2 mS/µm

## Slide 38: HEMT / MOS-HEMT State-of-the-Art
Institution | Device | Year | gm (mS/µm) | ft (GHz) | fmax (GHz) | √(ft•fmax)
Teledyne | HEMT | 2011 | 2.75 | 688 | 800 | 742
Tokyo Tech | HEMT | 2013 | 2.1 | 710 | 478 | 583
NGC | HEMT | 2015 | 3.1 | 610 | 1500 | 957
NTT | HEMT | 2019 | 2.8 | 703 | 820 | 759
Fraunhaufer | MOS-HEMT | 2019 | 2.4 | 275 | 640 | 420
UCSB Gen. 0 | MOS-HEMT | 2018 | 1.5 | 357 | 410 | 383
UCSB Gen. 1 | MOS-HEMT | 2019 | 2.3 | 511 | 256 | 361
UCSB Gen. 2 | MOS-HEMT | 2019 | 1.6 | 356 | 403 | 379
UCSB Gen. 3 | MOS-HEMT | 2020 | 2.9 | 406 | 562 | 477

## Slide 39: MOS-HEMT Future Work
Peak fꚍ severely limited by large CGS,p  need a self-aligned process
Peak fmax limited by large RG (poor yield & reproducibility)  improve T-Gate process
Develop > 1 x 1019 cm-3 In0.52Al0.48As for link region top barrier
Elegantly *hopefully* solved in one simple process

## Slide 40: MOS-HEMT Future Work

## Slide 41: MOS-HEMT Future Work
Advantages
Larger T-Gate aperture
Improved RG
Self-aligned Gate-Recess and T-Gate foot
Self-aligned ohmics possible
Disadvantages
Etching (dry & wet) in critical regions
Topography on wafer before critical dimension definition
Regrowth dynamics