## Slide 1: 200 GHz Low Noise Amplifiers in 250 nm InP HBT Technology
Utku Soylu
Affiliation: ECE, University of California, Santa Barbara, USA
Email address: utkusoylu@ucsb.edu
A. S. H. Ahmed1, M. Seo2, A. Farid1, M. Rodwell1
1ECE, University of California, Santa Barbara, USA
2ECE, Sungkyunkwan University, South Korea

## Slide 2: Outline
Motivation
Amplifier design
  - Noise measure technique
  - Low-loss input matching
Measurement results
Application of the amplifier
Summary

## Slide 3: Motivation
Increasing interest in the 200-300 GHz:
Large available BW  High data rate
Greater integration scales in SiGe/InP HBT receivers than in III-V HEMT technologies
More competitive 200-300 GHz all-HBT Rx with reduced HBT LNA noise figure
Ideal Case:
Hybrid Rx with HEMT LNA + HBT post-LNA

## Slide 4: 250 nm InP HBT Process (Teledyne [1])
Four Au interconnect.
TFR (50Ω/square).
MIM cap (0.3fF/µm2).
fmax=650GHz.
Jmax=3mA/µm.
BVCEo=4.5V.
MET4 = Signal, MET1 = GND
Loss of MSL = 1.1 dB/mm @ 200 GHz
Loss of inv-MSL = 2.5 dB/mm @ 200 GHz
Cross Section of TSC250 IC

## Slide 5: Noise Measure
[14] H. Fukui, "Available Power Gain, Noise Figure, and Noise Measure of Two-Ports and Their Graphical Representations," in IEEE Transactions on Circuit Theory, vol. 13, no. 2, pp. 137-142, June 1966.
Minimum Noise Measure Impedance:
Draw a line between centers of NF and Ga Circles.
Calculate M for each point on this line.
Determine the point on the line having the smallest M
Data is for an (0.25 x 5 μm^2) HBT in CB configuration with 200 fF base capacitance biased at VCB=0.4 V and JE=0.5 mA/μm

## Slide 6: Determining Bias Condition
FCASCADE,MIN=6.7 dB
FCASCADE,MIN as a function of emitter current density (JE) and collector-base voltage (VCB) for a 0.25 mm x 5 mm HBT.

## Slide 7: Noise Measure as a 2-port Invariant
[10] H. A. Haus and R. B. Adler, "Optimum Noise Performance of Linear Amplifiers," in Proceedings of the IRE, vol. 46, no. 8, pp. 1517-1533, Aug. 1958.
Minimum M is independent of circuit configuration;
Pick for high bandwidth or high gain/stage (=low PDC)
Data is for an (0.25 x 3 μm^2) HBT in CE configuration biased at VCB=0.4 V and JE=0.5 mA/μm
Emitter Inductance in CE
Base Capacitance in CB

## Slide 8: Input/Output Matching Matching
0.25 x 5 μm^2
VCB=0.4 V JE=0.5 mA/μm
0.25 x 3 μm^2
VCB=0.4 V JE=0.5 mA/μm

## Slide 9: Cascading
As we cascade more stages:
NFMIN converges to FCASCADE
Minimum NF impedance converges to Minimum NM impedance
1 stage, CE
2 stage, CE
3 stage, CE

## Slide 10: CB and CE Low Noise Amplifiers
200GHz | CB, 5um, 2 stage
Gain | 14.5 dB
BW | 33 GHz
NF | 7.4 dB
P1dB,in | -21.1 dBm
PDC | 9.2 mW
Die Area | 290umx245um
Jemitter Vcb | 0.6mA/um 0.4V
200GHz | CE, 5um, 4 stage
Gain | 13 dB
BW | 60 GHz
NF | 7.2 dB
P1dB,in | -18.2 dBm
PDC | 19.22 mW
Die Area | 290umx465um
Jemitter Vcb | 1.0mA/um 0.56V

## Slide 11: Measurement Results: S-parameters
WR-03 frequency extenders and probes, SOLT calibration
5 % frequency down-shift
Good agreement between peak simulated and measured gain
CB
CE

## Slide 12: Setup: Noise Measurement
Hot/Cold Y-parameter method (VDI-WR5.1NS noise source)
The probe loss (2.0 dB @ 200 GHz) and is deembedded from NF
~20 dB BB LNA used to reduce noise contribution from SA

## Slide 13: Measurement Results: Noise Figure
CB
CE
CB: 7.4±0.7 dB noise figure over 196-216 GHz
CE: 7.2±0.4 dB noise figure over 196-216 GHz

## Slide 14: Setup: Power Measurement
Simultaneous input and output power measurement
Accurate gain measurement even at low input power
All measurements are done without lifting the probes
[13] A. S. H. Ahmed, U. Soylu, M. Seo, M. Urteaga, J. F. Buckwalter and M. J. W. Rodwell., " A 190-210GHz Power Amplifier with 17.7-18.5dBm Output Power and 6.9-8.5% PAE.," in press, Proc. IMS2021.

## Slide 15: Measurement Results: Power
CB: -21.1 dBm Pin1dB @ 200 GHz
CE: -18.2 dBm Pin1dB @ 200 GHz

## Slide 16: Receiver with Staggered Tuned CB LNA
LNA: Normal microstrip for lowest NF
Mixer, LO multiplier, phase shifter: Inverted microstrip for low-inductance ground
3-stage staggered tuned CB LNA to increase 3 dB modulation bandwidth of the receiver
[14] M. Seo, A. S. H. Ahmed, U. Soylu, A. Farid, Y. Na and M. Rodwell, "A 200 GHz InP HBT Direct-Conversion LO-Phase-Shifted Transmitter/Receiver with 15 dBm Output Power," 2021 IEEE MTT-S International Microwave Symposium (IMS), 2021.
RF
LNA
RX I-Q mixer
Inverted microstrip
Normal microstrip
I
Q
0 o
90 o
25 GHz
x2
x2
x2
Phase
Shifter
LO multiplier
chain
200 GHz direct-conversion RX

## Slide 17: Measured Rx NF and Conversion Gain
Hot/Cold noise source
RX-IC
BB LNA
SA
VDI-WR5.1-NS
Noise Figure
Conversion Gain @ fixed fLO
Peak conversion gain = 22 dB
FCASCADE | 
5 um device | 6.7 dB
1-stage LNA | 7.5 dB
NF of Rx | 8.5-8.8 dB

## Slide 18: Performance Comparison
This work shows record Noise Figure in HBT technology.

## Slide 19: Acknowledgement
This work was supported by ComSenTer, a JUMP program sponsored by the Semiconductor Research Corporation.
The authors thank Teledyne Scientific & Imaging for the IC fabrication.

## Slide 20: Thank You!

## Slide 21: References
[1] M. J. W. Rodwell et al., “100-340GHz Systems: Transistors and Applications,” in Proc. IEEE IEDM, 2018, pp. 14.3.1-14.3.4
[2] Y. Zhao, E. Ojefors, K. Aufinger, T. F. Meister and U. R. Pfeiffer, "A 160-GHz Subharmonic Transmitter and Receiver Chipset in an SiGe HBT Technology," in IEEE Transactions on Microwave Theory and Techniques, vol. 60, no. 10, pp. 3286-3299, Oct. 2012.
[3] G. Moschetti et al., "A 183 GHz Metamorphic HEMT Low-Noise Amplifier With 3.5 dB Noise Figure," in IEEE Microwave and Wireless Components Letters, vol. 25, no. 9, pp. 618-620, Sept. 2015.
[4] A. Tessmann, A. Leuther, H. Massler, M. Kuri and R. Loesch, "A Metamorphic 220-320 GHz HEMT Amplifier MMIC," 2008 IEEE Compound Semiconductor Integrated Circuits Symposium, Monterey, CA, USA, 2008, pp. 1-4.
[5] Z. Wang, P. Chiang, P. Nazari, C. Wang, Z. Chen and P. Heydari, "A CMOS 210-GHz Fundamental Transceiver With OOK Modulation," in IEEE Journal of Solid- State Circuits, vol. 49, no. 3, pp. 564-580, March 2014.
[6] E. Ojefors, B. Heinemann and U. R. Pfeiffer, "Subharmonic 220- and 320-GHz SiGe HBT Receiver Front-Ends," in IEEE Transactions on Microwave Theory and Techniques, vol. 60, no. 5, pp. 1397-1404, May 2012.
[7] K. Eriksson, S. E. Gunnarsson, V. Vassilev and H. Zirath, "Design and Characterization of HH-Band (220–325 ~~GHz) Amplifiers in a 250-nm InP DHBT Technology," in IEEE Transactions on Terahertz Science and Technology, vol. 4, no. 1, pp. 56-64, Jan. 2014.
[8] J. Hacker et al., "THz MMICs based on InP HBT Technology," 2010 IEEE MTT-S International Microwave Symposium, Anaheim, CA, USA, 2010, pp. 1126-1129.
[9] M. Urteaga, Z. Griffith, M. Seo, J. Hacker, M. Rodwell, “InP HBT Technologies for THz Integrated Circuits”, Proceedings of the IEEE, Vol. 105, No. 6, pp 1051- 1067 June 2017.
[10] H. A. Haus and R. B. Adler, "Optimum Noise Performance of Linear Amplifiers," in Proceedings of the IRE, vol. 46, no. 8, pp. 1517-1533, Aug. 1958.
[11] A. Singhakowinta & A. R. Boothroyd, "Gain Capability of Two-port Amplifiers", International Journal of Electronics, Volume 21, Issue 6, 1966, pages 549-560.
[12] H. Fukui, "Available Power Gain, Noise Figure, and Noise Measure of Two-Ports and Their Graphical Representations," in IEEE Transactions on Circuit Theory, vol. 13, no. 2, pp. 137-142, June 1966.
[13] A. S. H. Ahmed, U. Soylu, M. Seo, M. Urteaga, J. F. Buckwalter and M. J. W. Rodwell., " A 190-210GHz Power Amplifier with 17.7-18.5dBm Output Power and 6.9-8.5% PAE.," in press, Proc. IMS2021.
[14] M. Seo, A. S. H. Ahmed, U. Soylu, A. Farid, Y. Na and M. Rodwell, "A 200 GHz InP HBT Direct-Conversion LO-Phase-Shifted Transmitter/Receiver with 15 dBm Output Power," 2021 IEEE MTT-S International Microwave Symposium (IMS), 2021.

## Slide 22: Setup: Noise Measurement (Pictures)

## Slide 23: Receiver Testing Setup
RF in
200 GHz
RX IC
BB out
8
Spectrum analyzer
20 dB coupler
Spectrum analyzer
Harmonic mixer
Freq. Multiplier
Var. attenuator
LO
Power meter
20 dB coupler
LO in
140-220 GHz (WR5) on-wafer testing
Simultaneous freq. & power testing
RX driven by multiplier & variable attenuator

## Slide 24: Measured Rx Power and Conversion Gain
Peak conversion gain = 22 dB
LO multiplier tuning bandwidth > 25 GHz
Conversion Gain @ fixed fBB
Pout vs Pin @ fLO=206 GHz (fBB=1 GHz)
Input P1dB = -24 dBm
Psat = +1 dBm
PDC = 825 mW

## Slide 25: Noise: HBT vs HEMT
By courtesy of Prof. Mark Rodwell

## Slide 26: CB and CE Low Noise Amplifiers
210GHz, Simulated | CB, 5um, 2 stage
Gain | 13.6 dB
BW | 33 GHz
NF | 7.4 dB
P1dB,in | -29.7 dBm
PDC | 9 mW
Die Area | 290umx245um
Jemitter Vcb | 0.6mA/um 0.4V
200GHz, Simulated | CE, 5um, 4 stage
Gain | 13.2 dB
BW | 60 GHz
NF | 8 dB
P1dB,in | -16.8 dBm
PDC | 19.2 mW
Die Area | 290umx465um
Jemitter Vcb | 1.0mA/um 0.56V