## Slide 1: Quasi-vdW epitaxy of GaAs on Si
Darshana Wickramaratne1, Y. Alaskar2,3, S. Arafin2, A. G. Norman4, Jin Zou5, Z. Zhang5, K.L Wang2, R. K. Lake1
1 Dept. of Electrical and Computer Engineering, UC Riverside, CA 92521, USA
2 Department of Electrical Engineering, UCLA, CA 90095, USA
3 King Abdulaziz City for Science and Technology, Riyadh 11442, Saudi Arabia
4 National Renewable Energy Laboratory, Denver, CO 80401, USA
5 Materials Engineering, The University of Queensland, St. Lucia, QLD 4072, Australia
Lawrence Epitaxy Workshop, Tempe, AZ 2015

## Slide 2
Heteroepitaxy
Challenges:
Surface dangling bonds/Surface states
Lattice mismatch
Polar on non-polar effects
Thermal expansion mismatch
...
GdTiO3/SrTiO3 superlattice
Phys. Rev. B 89, 075140, 2014
InP on amorphous SiO2
J Crystal Growth

## Slide 3
vdW gap
vdW gap
Proposed by Koma in 1984 for growth of NbSe2 on MoSe2. (Surface Science, 174(1), 556-560) Successfully adapted to other 2D materials
Low growth axis bond energies mitigates strain due to lattice mismatch
Challenges
Low surface energy of substrate
Low adsorption and migration energies
van-der-Waal epitaxy
Journ of Appl Phys vol 5, 5, 1999

## Slide 4
Quasi van-der-Waal epitaxy
Y Alaskar, et. al J Crystal Growth 2015

## Slide 5
Overview: Epitaxy on vdW Materials
Nano Lett. 2012, 12, 4570−457
Mixed phase growth of ZB and WZ
GaAs nanowires on graphene
Nano Lett. 2012, 12, 4570−457
InGaAs nanowire growth on graphene and
MoS2
J Appl. Phys. 74 (12), 1993
Growth of GaSe/GaAs on Si
Nature Comm. 5, 2014
Direct growth of WZ-GaN on graphene/SiC substrate

## Slide 6
Experimental Results
UCLA, NREL, Univ. Of Queensland, Y Alaskar, et. al, Adv Func Materials, 2014
Exfoliated Graphene

## Slide 7
Experimental Results cont’d...
CVD Graphene
Y Alaskar, et. al J Crystal Growth 2015

## Slide 8
Formalism
Density functional theory, slab supercell geometries
GaAs Band gap (eV) |  | 
Experiment | LDA | HSE
1.424 | 0.79 | 1.419
LDA bandgaps corrected for using hybrid HSE functional
vdW interactions accounted for using semi-empirical correction

## Slide 9
Graphene: Adsorption Energy and Migration Energy
 | Adsorption Site | Adsorption Energy - 2L (eV) | Adsorption Energy – 4L (eV) | Migration Energy – 2L(eV)
Ga | H | 1.5 | 1.53 | 0.05
Al | H | 1.7 | 1.72 | 0.03
In | H | 1.3 | 1.43 | 0.06
As | B | 1.3 | 1.28 | 0.21
N | B | 3.8 | 3.85 | 0.98
H-site
B-site

## Slide 10
MoS2 & h-BN: Adsorption and Migration Energy
 | Adsorption Energy |  |  | 
 | 1L h-BN (meV/atom) | 6L h-BN (meV/atom) | 1L-MoS2 (meV/atom) | 6L-MoS2 (meV/atom)
Ga | 131.6 (T) | 134.3 (T) | 234.6 (T) | 239.2 (T)
Al | 135.1 (T) | 101.1 (T) | 237.4 (T) | 241.6 (T)
In | 66.9 (B) | 85.1 (T) | 573.1 (T) | 582.1 (T)
As | 296.9 (B) | 341.5 (T) | 527.8 (T) | 537.8 (T)
Adsorption energies on monolayer and bilayer MoS2 and h-BN are an order
of magnitude lower compared to the adsorption energies on graphene
Weak hybridization of the III/V elements with the MoS2 and h-BN layers leads to low
adsorption energies

## Slide 11
Preferred phase and misorientation
Surface | Binding energy/C-atom (meV)
2x2 Reconstructed ZB GaAs(111) | -65.88
√19x√19 Reconstructed ZB GaAs(111) | -64.21
Wurtzite GaAs (0001) | -30.11
Ga
As

## Slide 12
Summary and Conclusions
Experimental demonstration of 25 nm thick GaAs(111) Si/SiO2/Graphene substrate using quasi van der Waal epitaxy
XRD indicates strong 111 orientation of GaAs on CVD grown graphene
DFT calculations indicate graphene is a superior vdW buffer layer compared to MoS2 and h-BN
Reconstructed GaAs(111) interface with graphene is preferred over WZ GaAs(0001)