## Slide 1: Device, Circuit, and Systems Considerations for Highly Integrated 30-300GHz Wireless Systems
Mark Rodwell, University of California, Santa Barbara
Short Course, IEEE BCICTS Conference, San Diego, October 14, 2018

## Slide 2: Why mm-wave wireless ?
Wireless networks: exploding demand.
Immediate industry response: 5G. 28, 38, 57-71(WiGig), 71-86GHz increased spectrum, extensive beamforming
Next generation (6G ??): above 100GHz.. greatly increased spectrum, massive spectral multiplexing
DOD applications: Imaging/sensing/radar, comms.

## Slide 3: A very incomplete history of THz electronics
1950-1990: THz GaAs Schottky diodes in waveguide Multipliers and mixers. Radio astronomy. Instruments. Spectroscopy.
1980's: THz spectroscopy using fs/ps pulsed lasers ps/fs pulsed lasers, optical/electrical conversion, time-domain techniques "optics is fast; electronics is slow"
1985-95: ps pulses using GaAs NLTLs + diode sampling ICs 100GHz commercial sampling scopes, fast network analyzers. 1995-2010: THz transistors, THz ICs Can we make transistors work at 1THz ? Abandon classical electrostatic barriers for quantum transitions ? Can circuit concepts work at 1THz ? (of course, just need D<<l !)
Dead end: Detecting poison gas

## Slide 4: mm-waves: high-capacity mobile communications
Gigabit mobile communication: Information anywhere, any time, without limits
Residential/office communication: Cellular/internet convergence: competition, low cost, broader deployment

## Slide 5: mm-wave imaging: fog/clouds/smoke/dust

## Slide 6: mm-waves: benefits & challenges
Massive # parallel channels
Need mesh networks
Need phased arrays (overcome high attenuation)
Large available spectrum
line-of-sight MIMO
spatial multiplexing
(note high attenuation in foul or humid weather)

## Slide 7: mm-waves: potential applications
High-capacity hubs massive spatial multiplexing
High-capacity backhaul massive spatial multiplexing
High-resolution imaging drive through fog/rain/snow
Compact imaging: drones image through fog/smoke/rain

## Slide 8
mm-wave fundamentals

## Slide 9: mm-Wave Wireless Needs Phased Arrays
isotropic antenna → weak signal →short range
highly directional antenna → strong signal, must be aimed
no good for mobile
beam steering arrays → strong signal, steerable
32-element array → 30 (45?) dB increased SNR
must be precisely aimed →too expensive for telecom operators

## Slide 10: Antenna & array basics

## Slide 11: Electronic beamsteering, a.k.a. phased array

## Slide 12: Multipath propagation: fading & ISI
(Delay spread<< symbol period ): fading LOS, NLOS arrive with aligned symbol periods. LOS, NLOS possibly out-of-phase: weak signal.
(Delay spread ≥ symbol period ): ISI One bit period interferes with another. Need adaptive equalization or OFDM.

## Slide 13: Beamforming can suppress ISI
1 Gbaud with 10o array beamwidth : multipath mostly causes fading not much ISI
10 Gbaud with 10o array beamwidth : significant fading and significant ISI
Solution 1: adaptive equalization or ODFM cost, complexity @ high rates ?
Solution 2: larger arrays narrower beamwidth

## Slide 14: Propagation, rain or shine
Rain: 10-3: 25mm/hr, 11dB/km 10-4: 50-85mm/hr, 19dB/km 10-5: 100+mm/hr: 30dB/km
35oC, 95% Humidity loss (dB/km)~(frequency/60GHz)2 11 dB/km@200 GHz, 5.5dB/km@140GHz
Extreme Fog (1g/m3) ~(25 dB/km)x(frequency/500 GHz)
Rosker, Wallace, 2007 IEEE International microwave symposium Olsen, Rogers, Hodge, IEEE Trans Antennas & Propagation Mar 1978 Liebe, Manabe, Hufford, IEEE Trans Antennas and Propagation, Dec. 1989 Liebe, IEEE Trans Ant and Pro, Vol 31, No. 1, Jan 1983 Karasawa, Maekawa, IEEE Proc, Vol 85 , #6 , June 1997

## Slide 15: Atmospheric Attenuation: Implications
Hardware favors lower frequencies Propagation environment is similar for 50-250GHz links ...but don't forget l2/R2 term ! Exclusive use of VLSI Si processes would force use of ~ < 180GHz
Worst-case attenuation: ~constant over 50-250 GHz. 10-5 outage rate: equal losses over 50-300 GHz 10-3 outage rate: equal losses over 50-200 GHz

## Slide 16
140-340 GHz: Possible Systems

## Slide 17: Spatial Multiplexing: massive capacity RF networks
multiple independent beams each carrying different data each independently aimed # beams approaches # array elements small: 1000 elements @220 GHz=3 square inches
Hardware: multi-beam phased array ICs

## Slide 18: mm-Wave LOS MIMO: multi-channel for high capacity
Massive capacity wireless; physically small
Torklinson : 2006 Allerton Conference Sheldon : 2010 IEEE APS-URSI Torklinson : 2011 IEEE Trans Wireless Comm.

## Slide 19: mm-wave imaging: TV-like resolution, small array
What you see in fog
What 10GHz radar shows
What you want to see
goal: ~0.2o resolution, 103-106 pixels
NxN phased array
mm-waves → high resolution from small antenna apertures
angular resolution = l /D (radians) 340 GHz, 35 cm/14 inch aperture → 0.14 degree resolution
D
D
HDTV-like resolution, fits on car, plane, UAV

## Slide 20: 140 GHz spatially multiplexed base station
1 Tb/s spatially-multiplexed base station 256 users/face, 4 faces 1024 total users @ 1 user/beam, 1 Gb/s/beam; 225 m range
Link budget is feasible, but... Required component dynamic range ? Required complexity of back-end beamformer ?
Handset: 8 × 8 array (9×9mm)

## Slide 21: 140 GHz spatially multiplexed base station
Each face supports 256 beams @ 1Gb/s/beam.
225 meters range in 50 mm/hr rain
PAs: 16 dBm Pout (per element)
LNAs: 3 dB noise figure
Realistic packaging loss, operating & design margins (20dB total)

## Slide 22: 140 GHz spatially multiplexed base station

## Slide 23: 75 GHz spatially multiplexed base station
If we use instead a 75GHz carrier, the range increases to 325 meters (vs. 250 meters) but the handset becomes 16mm×16mm (vs. 9mm×9mm), and the hub array becomes 9mm×655mm (vs. 5mm×350mm)
Or, use a 4×4 (8mm×8mm) handset array, and the range becomes 210 meters.

## Slide 24: 75GHz or 140GHz spatially multiplexed femtocells

## Slide 25: 340 GHz (or even 650 GHz) backhaul
Sub-mm-wave line-of-sight MIMO network backbone wireless @ optical speed; link network where fiber is too expensive to place. 340 GHz: 640Gb/s @ 500 meters range; 1.6 meter linear array (5Tb/s for 8×8 square array). 650 GHz: 1.28Tb/s @ 500 meter range; 1.6 meter linear array. Capacity doubles again if we use both polarizations.
linear array
square array

## Slide 26: 340 GHz 640 Gb/s MIMO backhaul
1.6m MIMO array: 8-elements, each 80 Gb/s QPSK; 640Gb/s total 4 × 4 sub-arrays → 8 degree beamsteering
500 meters range in 50 mm/hr rain; 29 dB/km
PAs: 82mW Pout (per element)
LNAs: 4 dB noise figure
Realistic packaging loss, operating & design margins

## Slide 27: 340 GHz 640 Gb/s MIMO backhaul

## Slide 28: 340 GHz 5 Tb/s MIMO backhaul
requires 10mW output per element ...10W total radiated power

## Slide 29: 140 GHz, 640 Gb/s MIMO backhaul
8-element 640Gb/s linear array: same link assumptions requires 2mW (vs. 80mW) power/element requires 2.6m (vs. 1.6m) linear array
Why not use a lower-frequency carrier, e.g. 140 GHz ?
8-element 5Tb/s square array: same link assumptions requires 0.25mW (vs. 10mW) power/element requires 2.6m (vs. 1.6m) square array

## Slide 30: 340 GHz frequency-scanned imaging car radar
Imaging for cars, aircraft drive safely @ 65MPH in heavy fog fly in heavy dust/fog/smoke
Short wavelengths: HDTV-resolution imaging, small: helicopter, drone, car
The challenge: complexity standard array: # pixels = # RF channels HDTV image: ~2×106 pixels. Need 2×106 RF channels !
Hardware-efficient imaging # RF channels << # pixels several techniques

## Slide 31: 340 GHz frequency-scanned imaging car radar
Image refresh rate: 60 Hz
Resolution 64×512 pixels
Angular resolution: 0.14 degrees
Aperture: 35 cm by 35 cm
Angular field of view: 9 by 73 degrees
Component requirements: 44 mW peak power/element, 3% pulse duty factor 6 dB noise figure, 3 dB package losses (each: trx, rcvr) 5 dB manufacturing/aging margin
See a soccer ball at 300 meters in heavy fog (10 seconds warning @ 100 km/hr.) (5 dB SNR, 35 dB/km, 30cm diameter target, 10% reflectivity)

## Slide 32: 340 GHz frequency-scanned imaging car radar

## Slide 33: mm-wave imaging with crossed linear arrays
Established approach.
Transmitter illuminates vertical stripe. Receiver detects horizontal stripe.
Requires 1×N arrays to form N×N image.
N2:1 SNR degradation with single-beam receiver Only 1/N of transmitter power is detected Receiver directivity is N:1 smaller than if focused on one image pixel
N1:1 SNR degradation with multi-beam receiver Receiver detects all transmitter power Receiver directivity is N:1 smaller than if focused on one image pixel

## Slide 34
Transistors

## Slide 35: mm-Wave Wireless Transceiver Architecture
custom PAs, LNAs → power, efficiency, noise Si CMOS beamformer→ integration scale
...similar to today's cell phones.

## Slide 36: IC Technologies for 100 + GHz systems
Silicon baseband processing at all frequencies RF sections @ 140, 200GHz PAs, LNAs in short-range 140, 220 GHz links GaN high-power amplifiers in long-range 140,220GHz links (possibly 340GHz ?)
InP HEMT low-noise amplifiers in long-range 140,220GHz links low-noise amplifiers @ 340, 650GHz
InP HBT medium-power amplifiers in long-range 140,220GHz links power amplifiers @340, 650GHz RF sections @ 340, 650GHz
Point-point MIMO: 340GHz: F= 4dB, Pavg=9.9dBm, Psat≅13.9dBm 650GHz: F= 4dB, Pavg=14.5dBm, Psat≅18.5dBm?
MIMO hub: 140GHz: F= 4dB, Pavg=17.5dBm, Psat≅21.5dBm 220GHz: F= 4dB, Pavg=21dBm, Psat≅25dBm

## Slide 37: mm-wave CMOS (UCSB examples)
150 GHz amplifier: IBM 65 nm bulk CMOS, 2.7dB gain per stage Seo et al., JSSC, Dec. 2009
145 GHz amplifier GF 45 nm SOI CMOS, 6.3 dB gain per stage Kim, Simseck, 2017 BCICTS

## Slide 38: 140GHz MIMO transceiver front-end ICs
S. Lee, A. Simseck, UCSB, 2018 BCICTS, to be presented

## Slide 39: mm-Wave CMOS won't scale much further
Gate dielectric can't be thinned → on-current, gm can't increase
Tungsten via resistances reduce the gain
Inac et al, CSICS 2011
Shorter gates give no less capacitance dominated by ends; ~1fF/mm total
Maximum gm, minimum C→ upper limit on ft. about 350-400 GHz.
Present finFETs have yet larger end capacitances

## Slide 40: III-V high-power transmitters, low-noise receivers
Cell phones & WiFi: GaAs PAs, LNAs
mm-wave links need: high transmit power, low receiver noise
0.47 W @86GHz
0.18 W @220GHz
1.9mW @585GHz
M Seo, TSC, IMS 2013
T Reed, UCSB, CSICS 2013
H Park, UCSB, IMS 2014

## Slide 41: Gallium Nitride Power Technologies
N-polar GaN: Mishra
GaN is the leading high-frequency power technology

## Slide 42: 130nm / 1.1THz InP HBT Technology
Teledyne: M. Urteaga et al: 2011 DRC
Rode (UCSB), IEEE TED, 2015
3.5 V breakdown

## Slide 43: 130nm / 1.1THz InP HBT: IC Examples
Teledyne: M. Urteaga et al: 2017 IEEE Proceedings
Integrated ~600GHz transmitter
220 GHz 0.18W power amplifier
UCSB/Teledyne: T. Reed et al: 2013 CSICS
325 GHz, 16mW power amplifier
UCSB/Teledyne: A. Ahmed, 2018 EuMIC Symp.
but, only ~1 mW output power

## Slide 44: Transistor scaling laws: ( V,I,R,C,t ) vs. geometry
Bulk and Contact Resistances
Depletion Layers
Thermal Resistance
Fringing Capacitances
Available quantum states to carry current
→ capacitance, transconductance contact resistance

## Slide 45
Frequency Limits and Scaling Laws of (most) Electron Devices
To double bandwidth: Reduce thicknesses 2:1 Improve contacts 4:1 Reduce width 4:1, Keep constant length Increase current density 4:1
PIN photodiode

## Slide 46: Bipolar Transistor Design

## Slide 47: Bipolar Transistor Design: Scaling

## Slide 48: Why InP Bipolar Transistors ?
InP: better electron transport than Si higher electron velocity: 3.5 vs 1.0 × 107 cm/s plus wider bandgap→ higher breakdown field
InGaAs base, base-emitter heterojunction: very low base sheet resistance
Implications: Higher (ft, fmax) at a given scaling node Higher breakdown* at a given (ft, fmax)
*Breakdown is too complicated to summarize with BVCEO. BVCBO vs. BVCEO vs. safe operating area ? Bottom line: look at Vce used in published IC data for a given IC technology.

## Slide 49: Making faster bipolar transistors
to double the bandwidth: | change
emitter & collector junction widths | decrease 4:1
current density (mA/mm2) | increase 4:1
current density (mA/mm) | constant
collector depletion thickness | decrease 2:1
base thickness | decrease 1.4:1
emitter & base contact resistivities | decrease 4:1
Narrow junctions. Thin layers High current density Ultra low resistivity contacts
Teledyne: M. Urteaga et al: 2011 DRC

## Slide 50: Refractory Ohmic Contacts to In(Ga)As
Refractory: robust under high-current operation / Low penetration depth: ~ 1 nm
32 nm (2.8THz) node requirements
Baraskar et al, Journal of Applied Physics, 2013
Why no ~2THz HBTs today? Problem: reproducing these base contacts in full HBT process flow

## Slide 51: THz HBTs: The key challenges
Obtaining good base contacts in HBT vs. in contact test structure (emitter contacts are fine)
Baraskar et al, Journal of Applied Physics, 2013
RC parasitics along finger length metal resistance, excess junction areas

## Slide 52
InP HBTs: 1.07 THz @200nm, ?? @ 130nm
?
Rode et al., IEEE TED, Aug. 2015

## Slide 53: 130nm /1.1 THz InP HBT ICs to 670 GHz
614 GHz fundamental VCO
340 GHz dynamic frequency divider
620 GHz, 20 dB gain amplifier
M Seo, TSC IMS 2013
also: 670GHz amplifier J. Hacker , TSC IMS 2013 (not shown)
M. Seo, TSC / UCSB
M. Seo, UCSB/TSC IMS 2010
204 GHz static frequency divider (ECL master-slave latch)
Z. Griffith, TSC / UCSB CSIC 2010
300 GHz fundamental PLL
M. Seo, TSC IMS 2011
220 GHz 180 mW power amplifier
T. Reed, UCSB CSICS 2013
600 GHz Integrated Transmitter PLL + Mixer
M. Seo TSC
Integrated 300/350GHz Receivers: LNA/Mixer/VCO
M. Seo TSC
81 GHz 470 mW power amplifier
H-C Park UCSB IMS 2014

## Slide 54: Towards a 2 THz SiGe Bipolar Transistor
 | InP | SiGe | 
emitter |  |  | 
junction width | 64 | 18 | nm
access resistivity | 2 | 0.6 | W-mm2
base |  |  | 
contact width | 64 | 18 | nm
contact resistivity | 2.5 | 0.7 | W-mm2
collector |  |  | 
thickness | 53 | 15 | nm
current density | 36 | 125 | mA/mm2
breakdown | 2.75 | 1.3? | V
ft | 1000 | 1000 | GHz
fmax | 2000 | 2000 | GHz
Similar scaling InP: 3:1 higher collector velocity SiGe: good contacts, buried oxides
Key distinction: Breakdown
InP has: thicker collector at same ft, wider collector bandgap
Key requirements:
low resistivity Ohmic contacts note the high current densities
Assumes collector junction 3:1 wider than emitter.
Assumes SiGe contacts no wider than junctions

## Slide 55: Towards the 2 THz / 64nm Node: 1st step = scaling
Narrow junctions. Thin semiconductor layers High current density Ultra low resistivity contacts
Yihao Fang, UCSB, submitted to DRC 2018
Initial DC data with 90nm devices

## Slide 56: FETs (HEMTs): key for low noise
2:1 to 4:1 increase in ft : improved noise less required transmit power smaller PAs, less DC power
or higher-frequency systems

## Slide 57: InP HEMTs: state of the art
Xiaobing Mei, et al, IEEE EDL, April 2015 (Northrop-Grumman)
First Demonstration of Amplification at 1 THz Using 25-nm InP High Electron Mobility Transistor Process

## Slide 58: FET Scaling Laws (these now broken)
FET parameter | change
gate length | decrease 2:1
current density (mA/mm) | increase 2:1
specific transconductance (mS/mm) | increase 2:1
transport mass | constant
2DEG electron density | increase 2:1
gate-channel capacitance density | increase 2:1
dielectric equivalent thickness | decrease 2:1
channel thickness | decrease 2:1
channel state density | increase 2:1
contact resistivities | decrease 4:1

## Slide 59: FET Scaling Laws (these now broken)
FET parameter | change
gate length | decrease 2:1
current density (mA/mm) | increase 2:1
specific transconductance (mS/mm) | increase 2:1
transport mass | constant
2DEG electron density | increase 2:1
gate-channel capacitance density | increase 2:1
dielectric equivalent thickness | decrease 2:1
channel thickness | decrease 2:1
channel state density | increase 2:1
contact resistivities | decrease 4:1
Gate dielectric can't be much further scaled. Not in CMOS VLSI, not in mm-wave HEMTs
gm/Wg (mS/mm) hard to increase→ Cend / gm prevents ft scaling.
Shorter gate lengths degrade electrostatics→ reduced gm /Gds → reduced fmax , ft

## Slide 60
Towards faster HEMTs
Scaling limit: gate insulator thickness HEMT: InAlAs barrier: tunneling, thermionic leakage solution: replace InAlAs with high-K dielectric 2nm ZrO2 (er=25): adequately low leakage
Scaling limit: source access resistance HEMT: InAlAs barrier is under N+ source/drain solution: regrowth, place N+ layer on InAs channel Target ~10nm node ~0.3nm EOT, 3nm thick channel 1.2 to 1.5 THz ft.

## Slide 61
Towards faster HEMTs: 1st results
Jun Wu, UCSB, IEEE EDL, 2018
Double regrowth modulation-doped access regions N+ contacts
High-K gate dielectric 3 nm ZrO2.
Highly scaled 5nm InAs channel 10-30nm gate lengths
Things to fix S/D contacts too far from gate widegap barrier under N+ S/D gate too wide: landed partly on access regions

## Slide 62: Towards faster HEMTs: next step
Jun Wu, UCSB, Unpublished
Revised process: no N- material between channel and contacts reduced source/drain access resistance
Revised process: sacrificial layer reduces parasitic gate-channel overlap: less gate-source capacitance
Thinner gate dielectric (2nm ZrO2), thinner channel (3nm InAs) higher gm , lower gds

## Slide 63
ICs

## Slide 64: mm-Wave IC design: the challenges
Transistor gains are low: fsignal is significant fraction of fmax. usually must match for optimum gain, noise, or power.
(Transistor, resistor, capacitor) dimensions are a significant fraction of a wavelength Even short lengths of random wiring add serious inductance and/or capacitance
Transmission-line losses are high low Q in VCO resonators and filters high combining losses in PAs: low power, low efficiency several dB added noise in LNAs.
First consider the IC wiring stack (the next 5-6 slides are very old, predate modern mm-wave CMOS)

## Slide 65: III-V MIMIC Interconnects: Classic Substrate Microstrip
kz
Strong coupling when substrate approaches ~ld / 4 thickness
H
W
Thick Substrate → low skin loss
Zero ground inductance in package
High via inductance
12 pH for 100 mm substrate -- 7.5 W @ 100 GHz
TM substrate mode coupling
Line spacings must be ~3*(substrate thickness)
lines must be widely spaced
ground vias must be widely spaced
all factors require very thin substrates for >100 GHz ICs → lapping to ~50 mm substrate thickness typical for 100+ GHz
No ground plane breaks in IC

## Slide 66: Coplanar Waveguide
kz
Parasitic slot mode
-V
0V
+V
0V
No ground vias No need (???) to thin substrate
Parasitic microstrip mode
+V
+V
+V
0V
Hard to ground IC to package
substrate mode coupling or substrate losses
ground plane breaks → loss of ground integrity
Repairing ground plane with ground straps is effective only in simple ICs In more complex CPW ICs, ground plane rapidly vanishes → common-lead inductance → strong circuit-circuit coupling
40 Gb/s differential TWA modulator driver note CPW lines, fragmented ground plane
35 GHz master-slave latch in CPW note fragmented ground plane
175 GHz tuned amplifier in CPW note fragmented ground plane
poor ground integrity
loss of impedance control
ground bounce
coupling, EMI, oscillation
III-V: semi-insulating substrate→ substrate mode coupling
Silicon conducting substrate → substrate conductivity losses

## Slide 67: If It Has Breaks, It Is Not A Ground Plane !
signal line
signal line
ground plane
coupling / EMI due to poor ground system integrity is common in high-frequency systems whether on PC boards ...or on ICs.

## Slide 68: No clean ground return ? → interconnects hard to model
35 GHz static divider interconnects have no clear local ground return interconnect inductance is non-local interconnect inductance has no compact model
InP 8 GHz clock rate delta-sigma ADC
8 GHz clock-rate delta-sigma ADC thin-film microstrip wiring every interconnect can be modeled as microstrip some interconnects are terminated in their Zo some interconnects are not terminated ...but ALL are precisely modeled

## Slide 69: III-V MIMIC Interconnects: Thin-Film Microstrip
fewer breaks in ground plane than CPW
narrow line spacing → IC density
... but ground breaks at device placements
still have problem with package grounding
thin dielectrics → narrow lines → high line losses → low current capability → no high-Zo lines
H
W
...need to flip-chip bond
no substrate radiation, no substrate losses
InP 34 GHz PA (Jon Hacker , Teledyne)

## Slide 70: III-V MIMIC Interconnects: Inverted Thin-Film Microstrip
No breaks in ground plane
narrow line spacing → IC density
... no ground breaks at device placements
still have problem with package grounding
thin dielectrics → narrow lines → high line losses → low current capability → no high-Zo lines
...need to flip-chip bond
Some substrate radiation / substrate losses
InP 150 GHz master-slave latch
InP 8 GHz clock rate delta-sigma ADC

## Slide 71: VLSI mm-wave interconnects with ground integrity
negligible breaks in ground plane
narrow line spacing → IC density
negligible ground breaks @ device placements
still have problem with package grounding
thin dielectrics → narrow lines → high line losses → low current capability → no high-Zo lines
...need to flip-chip bond
no substrate radiation, no substrate losses
Also: Ground plane at *intermediate level* permits critical signal paths to cross supply lines, or other interconnects without coupling. (critical signal line is placed above ground, other lines and supplies are placed below ground)

## Slide 72: ICs in Thin-Film (Not Inverted) Microstrip
Note breaks in ground plane at transistors, resistors, capacitors Interconnects within these breaks will be more difficult to model.

## Slide 73: ICs in Thin-Film Inverted Microstrip
100 GHz differential TASTIS Amp. 512nm InP HBT

## Slide 74: ICs in Thin-Film Inverted Microstrip
8:1, 205 GHz static divider in 256 nm InP HBT. Image taken before top metal (ground plane) deposition
205 GHz divider, Griffith et al, IEEE CSIC, Oct. 2010

## Slide 75: High Speed ECL Design: transmission-lines
Followers associated with inputs, not outputs Emitters never drive long wires. (instability with capacitive load)
Double termination for least ringing, send or receive termination for moderate-length lines, high-Z loading saves power but kills speed.

## Slide 76: Power supply problems
Detuning of individual stages Coupling, feedback via supply→ oscillation, loss of path isolation
local resonances between bypass cap and supply interconnects global LC standing-wave resonances on supply bus

## Slide 77: Power supply problems
The supply impedance will detune individual stages.

## Slide 78: Power supply problems
Here, the supply is terminated by 50 Ohms through a bias T. This avoids resonances. More generally, we must simulate system for wide range of external supply impedance.
Model the supply in all simulations. "If it is on the {IC, PCB, probe station}, put it in the simulation."

## Slide 79: Differential mm-wave stages
Common-emitter
M. Seo, Teledyne
Common-base
M. Seo, 2013 IMS
Virtual ground→ avoids ground via inductance  Avoids power-supply coupling  Potential problems with common mode ✘

## Slide 80: Pseudo-Differential Stages

## Slide 81: RF-IC Design: Simple & Well-Known Procedures
1: (over)stabilize at the design frequency guided by stability circles
3: Tune remaining port for maximum gain
2: Tune input for Fmin (LNAs) or output for Psat (PAs)
4: Add out-of-band stabilization.
This seems simple: so where are the challenges ?

## Slide 82: mm-Wave IC design: the challenges
Transistor gains are low: fsignal is significant fraction of fmax. usually must match for optimum gain, noise, or power.
(Transistor, resistor, capacitor) dimensions are a significant fraction of a wavelength Even short lengths of random wiring add serious inductance and/or capacitance
Transmission-line losses are high low Q in VCO resonators and filters high combining losses in PAs: low power, low efficiency several dB added noise in LNAs.

## Slide 83: Multi-finger transistor cell layout

## Slide 84: Sub-mm-wave PAs: need more current
3 mm max emitter length (> 1 THz fmax) 2 mA/mm max current density: Imax= 6 mA Maximum 3 Volt p-p output Load: 3V/6mA= 500 W
Combiner cannot provide 500 W loading

## Slide 85: mm-wave PAs: need more current
InP HBTs: thinner collector→ more current hotter→ improve heat-sinking or: longer emitters→ thicker base metal
GaN HEMTs: much higher voltage 100+ GHz: large multi-finger FETs not feasible Need high current to exploit high voltage.
Need more mA/mm or longer fingers
Example: 2mA/mm, 100 mm max gate width, 50 Volts 200mA maximum current 50 Volts/200mA= 250 W load→ unrealizable.

## Slide 86: 4:1 series-connected 81GHz power amplifier
17 dB Gain, 470 mW Psat , 23% PAE Teledyne 250 nm InP HBT, 2 stages, 1.0 mm2(incl pads)
Park et al., 2014 IEEE-IMS

## Slide 87: 90 mW, 220 GHz Power Amplifier
Reed (UCSB) and Griffith (Teledyne): CSIC 2012. Teledyne 250 nm InP HBT
active area, 1.02 x 0.85 mm die: 2.42 x 1.22 mm

## Slide 88: 214 GHz, 180mW Power Amplifier (330 mW design)
2.3 mm x 2.5 mm
T. Reed, Z. Griffith, 2014 CSICS http://ieeexplore.ieee.org/xpls/abs_all.jsp?arnumber=6659187&tag=1

## Slide 89: 220GHz PA Design; in development
Unit cell
S21
S22
S11
Max Psat
Gain
Linearity
Technology: 250nm InP HBT
Combining techniques investigated:
  - Series, Balun, Wilkinson
  - Branched l/4 network 
Unit cells investigated
  - CE, Cascode
  - CB with grounded base
  - CB with optimized base impedance
Pout
PAE
Gain
Technology | 250-nm InP HBT
Freq, GHz | 205
#cells | 8
VCC, V | 2.25
Jbias,mA/um | 1.33
S21, dB | 15.9
Pout ,dBm | 17.8*, 20.7**
PAE % | 6.8*,12.9**
BW3dB, GHz | 35
area, µmµm | 750×717
*at 1dB compression, **at 2dB | 
Technology | 250-nm InP HBT
Freq, GHz | 205
#cells | 8
VCC, V | 2.25
Jbias,mA/um | 1.33
S21, dB | 15.9
Pout ,dBm | 17.8*, 20.7**
PAE % | 6.8*,12.9**
BW3dB, GHz | 35
 | 750×717
*at 1dB compression, **at 2dB | 
8 to 1 combiner
ONLY 0.7dB loss

## Slide 90: 370 GHz dynamic divider

## Slide 91: 570 GHz oscillator

## Slide 92: 326 GHz series-connected PA
16mW Psat; 1.3% PAE, 16.6dB gain
A. Ahmed, 2018 BCICTS

## Slide 93
Systems & Packages

## Slide 94: Beamforming for massive spatial multiplexing
Pure digital beamforming: dynamic range & phase noise requirements: both appear to be manageable  Digital back-end processing requirements (die area, DC power): being investigated ???
Pure RF beamforming: (focal plane, Butler matrixes, RF beamforming) Established approach in DOD systems (high dynamic range). Issues of array tiling.

## Slide 95: Large arrays formed from small tile models
Point-point MIMO, MIMO hub, imaging all require relative large arrays
Modular assembly large array formed from many small tiles

## Slide 96: The mm-wave module design problem
How to make the IC electronics fit ? 100+ GHz arrays: l0/2 element spacing is very small. Antennas on or above IC → IC channel spacing = antenna spacing → limited IC area to place circuits
How to avoid catastrophic signal distribution losses ? long-range, high-gain arrays: array size can be large. ICs beside array → very long wires between beam former and antenna → potential for very high signal distribution losses
How to remove the heat ? 100+ GHz arrays: element spacing is very small. If antenna spacing = IC channel spacing, then power density is very large

## Slide 97: mm-wave/sub-mm-wave packaging
Not all systems steer in two planes... ...some steer in only one.
Not all systems steer over 180 degrees... ...some steer a smaller angular range
Arrays can often be linear (1D), instead of rectangular (2D) Element spacing can often be greater than l/2.
→ Array packaging then greatly simplified.

## Slide 98: Background: split-block waveguides
Waveguides are manufactured (milled or die cast) from a set of pieces
Precision pins aid alignment

## Slide 99: Concept: Tile for mm-wave arrays
Split-block assembly. Modules tile into larger array
IC area can be much larger than antenna area→ electronics can fit
Low-loss waveguide feeds, efficient waveguide horn antennas
Efficient heat-sinking: permits W-level GaN, InP, SiGe PAs for long range

## Slide 100: Concept: Tile for linear arrays
Terrestrial system: horizontal steering only→ linear array. Space at edges of linear array: room for III-V PAs, LNAs. Alternating-sides feed: 2mm pitch→ room for large GaN PAs. Mounting directly on metal carrier→ heatsinking.

## Slide 101: Concept: module for small angular scanning
Terrestrial system: horizontal + vertical steering → rectangular array. Limited angular steering range (installation)→ spacing >> l/2 Endfire / edge-card geometry: room for III-V PAs, LNAs. Mounting directly on metal carrier→ heatsinking.
If Vivaldi's are replaced with dipoles, element spacing can be reduced to l/2. → potential for wider angular scanning

## Slide 102: Concept: module for handset
Handset transceiver performance: less challenging. No external III-V PAs, LNAs
Handset transceiver is simpler: single-beam, not spatially multiplexed Smaller die area→ array pixel fits in l/2 × l/2
Vertical integration of antenna on low-er superstrate. fused Silica (Rebeiz) possibly also: spin-cast BCB or polyimide, post-process.

## Slide 103
Wireless above 100GHz

## Slide 104: Wireless above 100 GHz
Massive capacities large available bandwidths massive spatial multiplexing in base stations and point-point links
Very short range: few 100 meters short wavelength, high atmospheric losses. Easily-blocked beams.
IC Technology All-silicon for short ranges below 250 GHz. III-V LNAs and PAs for longer-range links. Just like cell phones today III-V frequency extenders for 340GHz and beyond
The challenges spatial multiplexing: computational complexity, dynamic range packaging: fitting signal channels in very small areas