## Slide 1: Transistors: mm-Wave and Low-Power VLSI
Mark Rodwell, UCSB
Plenary, Compound Semiconductor Week, May 29th, 2018 - June 1st, 2018, MIT
InP HBT: Y. Fang, J. Rode*: UCSB
InP MOS-HEMT J. Wu: UCSB
Low-voltage devices B. Markman, H.-Y. Tseng, S. Brunelli, S. Choi, A. Goswani, C. Palmstrøm, J. Klamkin: UCSB P. Long, J. Huang, E. Wilson, S. Mehrotra, C.Y.-Chen, M. Povolotskyi, G. Klimeck: Purdue
Now with *Intel
Millimeter-wave systems design, mm-wave ICs. M. Abdelghany, A. Farid, A. Ahmed, U. Madhow : UCSB A. Niknejad: UC Berkeley

## Slide 2
VLSI Transistors
2

## Slide 3: Why is Moore's law scaling nearly over ?
Cannot make FET gates much shorter
Oxide tunneling: minimum oxide thickness → minimum gate length given electrostatics
Source-drain tunneling: minimum gate length
Power density: becoming excessive
CwireVDD2 switching energy: → want low VDD
Static leakage Ioff > Ionexp(-qVDD /kT) → want high VDD
Reducing gate length reduces power: integration density ↑, wiring capacitance ↓, switching energy ↓.
Reduce power by reducing voltage or increasing density

## Slide 4: 3D: increasing integration density
Planar FETs: 7nm node uses 15nm gate; can't get much shorter > 15nm minimum transistor pitch.
R. Xie et al., 2016 IEDM
If oriented vertically, minimum transistor pitch is ~6nm physical limit; fabrication might be difficult/impossible
Perhaps it can be done ?

## Slide 5: Tunnel FETs: truncating the thermal distribution
Source bandgap truncates thermal distribution
J. Appenzeller et al., IEEE TED, Dec. 2005
T-FET
Normal
Must cross bandgap: tunneling ✘
Fix (?): GaSb/InAs broken-gap heterojunction

## Slide 6: Tunnel FETs: are prospects good ?
For high Ion, tunnel barrier must be *very* thin.
Real TFET nonzero barrier energy: quantization nonzero barrier thickness: electrostatics

## Slide 7: TFET on-currents are low, TFET logic is slow
3.0%
NEMO simulation: GaSb/InAs tunnel finFET: 2nm thick body, 1nm thick dielectric @ er=12, 12nm Lg
10 mA/mm
Experimental: Tabulation from Zhao et al., MIT, IEEE EDL, 7/2017
Low current → slow logic

## Slide 8: [110] gives more on-current than [100]
high confinement mass low transport mass
low confinement mass high transport mass
P. Long et al., EDL 3/2016

## Slide 9: Heterojunctions increase the junction field.
Added heterojunctions→ greater built-in potential→greater field→ thinner barrier
Source HJ: S. Brocard, et al., EDL, 2/2014; Channel HJ: P. Long et al., EDL 3/2016
Key facts: 2nm thick channel, design for VDD=70mV.

## Slide 10: Heterojunctions increase the tunneling probability
Added heterojunctions→ greater built-in potential→greater field→ thinner barrier
Key facts: 2nm thick channel, design for VDD=70mV.
Source HJ: S. Brocard, et al., EDL, 2/2014; Channel HJ: P. Long et al., EDL 3/2016

## Slide 11: Heterojunctions increase the on-current
Added heterojunctions→ greater built-in potential→greater field→ thinner barrier
Key facts: 2nm thick channel, design for VDD=70mV.
Source HJ: S. Brocard, et al., EDL, 2/2014; Channel HJ: P. Long et al., EDL 3/2016

## Slide 12: Role of the resonant bound states
On-state: bound states increase transmission Off-sate: evanescent tails of bound states increases leakage → Keep the bound state energies near the well edge energies
P. Long et al., 2016 IEDM: Resonances in TFETs: Avci & Young (Intel) 2013 IEDM
local density of states, 1/eV

## Slide 13: Preferred semiconductors under gate dielectric
InGaAs: 64mV/dec.
InAs: 61mV/dec.
InP: 67*mV/dec.
*Note InP/InGaAs band offset
Lee et al., 2014 DRC
Lee et al., 2014 VLSI Symposium
Huang et al., 2014 Lester Eastman Conference
Gate dielectrics: Chobpattana et al. (Stemmer), APL 5/2014, APL 10/2014, Carter et al. (Rodwell) Applied Physics Express 8/2011

## Slide 14: Target 3HJ tunnel transistor design
Design Source well (NA=5×1019/cm3) Channel well 1) 4.0nm p-Ga0.47In0.53As 4.5nm i-Ga0.47In0.53As 2) 4.0nm p-Ga0.74In0.26As, 1.9% tensile strain 4.0nm i-Ga0.23In0.77As, 1.6% compressive strain 3) 4.0nm p-GaAs, 3.8% tensile strain 3.5nm i-InAs, 3.1% compressive strain
NA=5×1019/cm3
Design 3: highest current, no semiconductor alloys.
Need design revision: P-InP → P-InAlAs in source
Long et al., 2017 DRC

## Slide 15: Target 3HJ tunnel transistor design: simulations
Design Ballistic (SS, Ion @ Ioff=1nA/mm, VDD=0.3V) With phonon-assisted tunneling 1) 15mV/dec., 0.18mA/mm 20mV/dec., 0.14mA/mm 2) 14mV/dec., 0.43mA/mm 26mV/dec., 0.36mA/mm 3) 14mV/dec., 0.61mA/mm 34mV/dec., 0.39mA/mm
Design 3: highest current, no semiconductor alloys.
Long et al., 2017 DRC

## Slide 16: Base III-V MOS Technology at UCSB
C. Y. Huang et al., DRC 2015
Good DC MOSFET with 12nm Lg, 2.5 nm thick channel
22nm Lg: 0.5 mA/mm ION @ 100nA/mm IOFF & 0.5V VDD
S. Lee et al., VLSI 2014
V. Chobpattanna, S. Stemmer FET data: S Lee, 2014 VLSI Symp.
Gate dielectrics with very low trap density

## Slide 17: How to build the device? No easy approach.
Memišević, et al 2016 IEEE Silicon Nanoelectronics Workshop
Fujimatsu, Saito, Miyamoto, 2012 IEEE IPRM
Target growth & process flow: Template Assisted Selective Epitaxy (TASE)
All TFETs: need junction perpendicular to gate dielectric. how ?
Example processes:
gated mesa edge
nanowire
L. Czornomaz et al. (IBM Zurich ), 2015 & 2016 VLSI Symposia
vertical etched ridge

## Slide 18: TFETs by template-assisted epitaxy
TASE: L. Czornomaz et al. (IBM Zurich ), 2015 & 2016 VLSI Symposia
This conference: see paper Fr2B7, Nanostructures session, S. Brunelli et al., Towards Horizontal Heterojunctions ...

## Slide 19: MOCVD TASE
Chart: template length (µm)
| 6 | 7 | 8 | 9 | 10 | 11 | 12
1500 s | 682 | 588 | 473 | 414 | 374
2500 s | 1185 | 1160 | 1266 | 946 | 944 | 682 | 853 | 792 | 639 | 714 | 691 | 649 | 581 | 536 | 559
3500 s | 1120 | 1030 | 800 | 730 | 620
4500 s | 1358 | 1318 | 1192 | 1040 | 897 | 850 | 769 | 660 | 722
Growth in the template cavity appears to be limited by diffusion mechanisms
Template length influences growth rate with inverse proportionality
Summary of four growth runs of different time
This conference: see paper Fr2B7, Nanostructures session, S. Brunelli et al., Towards Horizontal Heterojunctions ...

## Slide 20: TFETs: horizontal heterojunctions by TASE
Heterojunctions by pseudo-ALE InP with ~1.25nm strained InAs layers 110 wafer, clean growth facets
This conference: see paper Fr2B7, Nanostructures session, S. Brunelli et al., Towards Horizontal Heterojunctions ...

## Slide 21: Horizontal InAs & GaAs heterojunctions in InP
Working now on better control of the layer thicknesses...

## Slide 22: Towards a TASE-fabricated TFET
First step: simple MOSFET with regrowth S/D contacts ALE-deposited gate dielectric and metals
Remaining steps for 3HJ-TFET horizontal GaAs/InAs/InP HJ P+ InGaAs doping ...growth & fabrication

## Slide 23: Alterative process: vertical ridge
Drain pads support narrow vertical ridge → target 5-10 nm ridge
Wrap-around gate wraps over drain no need for planarization
18nm fins

## Slide 24
THz transistors
24

## Slide 25: Transistors for mm-wave, sub-mm-wave wireless
Massive growth in use of radio communication sub-5GHz spectrum almost used up
Next generation 5G, coming soon. 28, 38, 57-71(WiGig), and 71-86GHz. Some degree of spatial multiplexing (multiple beams)
Research now explores the next generation (6G?). 100+ GHz carriers: 140, 220, 340GHz maybe 650GHz massive spatial multiplexing
This will drive transistor development: PAs for transmitters, GaN, InP HBT, SiGe HBT LNAs for receivers: InP HEMT, InP MOS-HEMT

## Slide 26: 100-340GHz wireless communications
Gigabit mobile communication.
Information anywhere, any time, without limits
Gigabit residential/office communication.
Cellular/internet convergence: competition, low cost, broader deployment

## Slide 27: 140/220 GHz spatially multiplexed base station
10 Tb/s spatially-multiplexed base station Each face supports 256 beams @ 10Gb/s/beam. 100 meters range in 50 mm/hr rain Realistic packaging loss, operating & design margins
Key device specifications: 140 GHz: PAs: Psat=21.5 dBm: LNAs: F=4 dB 220 GHz: PAs: Psat=25 dBm: LNAs: F=4 dB

## Slide 28: 340 GHz, 650 GHz spatially-multiplexed backhaul
340 GHz: 640Gb/s @ 240 meters; 1.2 meter, 8-element array F= 4dB, Psat≅14dBm
650 GHz: 1.28Tb/s @ 240 meters; 1.2 meter, 16-element array F= 4dB, Pavg=14.5dBm, Psat≅18.5dBm

## Slide 29: mm-Wave Wireless Transceiver Architecture
custom PAs, LNAs → power, efficiency, noise Si CMOS beamformer→ integration scale
...similar to today's cell phones.

## Slide 30: mm-wave CMOS (examples)
260 GHz amplifier, Feedback-enhanced-gain: 65nm bulk CMOS, 2.3 dB gain per stage (350GHz fmax) Momeni ISSCC, March 2013
145 GHz amplifier, conventional neutralized design: 45 nm SOI CMOS, 6.3 dB gain per stage, ~1.5mW Psat Kim et al. (UCSB), submitted
350 GHz fmax

## Slide 31: mm-Wave CMOS won't scale much further
Gate dielectric can't be thinned → on-current, gm can't increase
Tungsten via resistances reduce the gain
Inac et al, CSICS 2011
Shorter gates give no less capacitance dominated by ends; ~1fF/mm total
Maximum gm, minimum C→ upper limit on ft. about 350-400 GHz.
Present finFETs have yet larger end capacitances

## Slide 32: Gallium nitride mm-wave power
N-polar GaN: Mishra
nm AlN/GaN: Xing/Jena
GaN is the leading high-frequency power technology

## Slide 33: 130nm / 1.1THz InP HBT Technology
Teledyne: M. Urteaga et al: 2011 DRC
Rode (UCSB), IEEE TED, 2015
3.5 V breakdown

## Slide 34: THz transistor measurements
Problems with simple pads: Substrate resonances @ >35 GHz → make pads small, grounds close(!) Ambiguity in series-first or shunt-first pad stripping. Our present HBTs, stripping order makes only a minor difference.
On-wafer LRL is much better No pad-stripping. Still must avoid substrate resonances thinned substrate with TSV's or thin-film microstrip wiring
(publication used parallel elements outside)
220 mm

## Slide 35: 130nm / 1.1THz InP HBT: IC Examples
Teledyne: M. Urteaga et al: 2017 IEEE Proceedings
Integrated ~600GHz transmitter
220 GHz 0.18W power amplifier
UCSB/Teledyne: T. Reed et al: 2013 CSICS
325 GHz, 16mW power amplifier
UCSB/Teledyne: (A. Ahmed, submitted)
but, only ~1 mW output power

## Slide 36: InP HBT: Towards the 2 THz / 64nm Node
Yihao Fang, UCSB, to be submitted
Thin semiconductor layers (transit time) High current density (CV/I) Narrow junctions (heat) Ultra low resistivity contacts (RC) Low base metal resistance (RC) 5nm P+ spike: low-rc contacts, good b.
90 nm HBT
45 nm emitter

## Slide 37: InP HBT: Towards the 2 THz / 64nm Node
Yihao Fang, UCSB, to be submitted
Good b, even at 90nm.
...because of doping pulse, grade

## Slide 38: Challenges at 65nm: base contacts, base metal
Obtaining good base contacts in HBT vs. in contact test structure (emitter contacts are fine)
RC parasitics along finger length metal resistance, excess junction areas
Rode et al., IEEE TED, Aug. 2015
Baraskar et al, Journal of Applied Physics, 2013

## Slide 39: Challenges at 65nm: Base contact penetration
TLM test samples: ultra-clean surfaces non-penetrating contacts refractories: Ru, Mo, Ir, W → ~6×10-9 W-cm2 resistivity
HBT emitter: first process step ultra-clean surfaces refractory Mo contacts ~1-2×10-8 W-cm2 resistivity
HBT base: late process step UV-O3/HCl cleaning not enough controlled-penetration contacts: 1nm Pt→ 3nm reaction depth → incompatible with thin & pulse-doped base designs
Rode et al., IEEE TED, Aug. 2015

## Slide 40: Next: regrowth instead of scaling
Goal: regrown-base HBT increased b, fmax
Goal: pedestal-collector HBT increased fmax
1st step : collector growth in dielectric window
Next step: base lateral overgrowth,
or base confined lateral overgrowth
Intrinsic/extrinsic base junction metamorphic p-GaAs/p-InGaAs electron barrier→ high b low intrinsic doping→ low Auger→ high b

## Slide 41: mm-wave PAs: need higher current density
3 mm max emitter length (> 1 THz fmax) 2 mA/mm max current density Imax= 6 mA Maximum 3 Volt p-p output Load: 3V/6mA= 500 W
1) Transmission-line combiner: cannot provide 500 W loading 2) Lumped multi-finger layouts: parasitics, reduced gain, fmax

## Slide 42
HEMTs: key for low noise
Hand-derived modified Fukui Expression, fits CAD simulation extremely well.
2:1 to 4:1 increase in ft → improved noise
→ less required transmit power→ easier PAs, less DC power
or enable higher-frequency systems

## Slide 43: Towards faster HEMTs
Scaling limit: gate insulator thickness HEMT: InAlAs barrier: tunneling, thermionic leakage solution: replace InAlAs with high-K dielectric 2nm ZrO2 (er=25): adequately low leakage
Scaling limit: source access resistance HEMT: InAlAs barrier is under N+ source/drain solution: regrowth, placing N+ layer on InAs channel
Jun Wu, UCSB, IEEE EDL

## Slide 44
Towards faster HEMTs
Jun Wu, UCSB, IEEE EDL, 2018
Double regrowth modulation-doped access regions N+ contacts
High-K gate dielectric: 3 nm ZrO2.
Highly scaled 5nm InAs channel 10-30nm gate lengths

## Slide 45
Towards faster HEMTs: next step
Jun Wu, UCSB, Unpublished
Revised process: no N- material between channel and contacts reduced source/drain access resistance
Revised process: sacrificial layer reduces parasitic gate-channel overlap: less gate-source capacitance
Thinner gate dielectric (2nm ZrO2), thinner channel (3nm InAs) higher gm , lower gds

## Slide 46
Transistors: mm-Wave Low-Power VLSI
46

## Slide 47: Electron devices for VLSI
Low-voltage transistors low voltage → low CV2 → low switching power. NC FETs. high-current TFETs.
3D integration more transistors/cm2→smaller IC→ shorter wires→ less power process-intensive: can universities contribute ?
nm-scale memory easier than nm logic: don't need good Ion, Ioff at low VDD. just need to change a physical state, then measure it.

## Slide 48: nm and THz Transistors
The transistor was demonstrated 70 years ago. most easy things have been done. nm technologies need advanced tools: hard for universities. what should we do next ?
VLSI low voltage logic: NCFETs, high-current TFETs 3D integration. atomic-scale memory.
High-frequency transistors: 100-340GHz power transistors: GaN HEMT, InP HBT low-noise transistors: InP HEMT Beyond-220GHz transistors: InP HBT & HEMT
Power conversion and control.

## Slide 49
(backup slides follow)

## Slide 50: 100-340 GHz: benefits & challenges
Massive # parallel channels
Need mesh networks
Need phased arrays (overcome high attenuation)
Large available spectrum
line-of-sight MIMO
spatial multiplexing
(note high attenuation in foul or humid weather)

## Slide 51: 100-340GHz: radar and imaging
340 GHz TV-resolution radar: see through fog and rain. drive safely in fog at 100 km/hr self-driving: complements LIDAR, but works in bad weather
60 GHz Doppler / ranging radar. long-range but low-resolution: detects objects, but can't recognize them .
Imaging for drones, small aircraft small, light aperture, high resolution.

## Slide 52: Effect of order of pad stripping

## Slide 53: Effect of order of pad stripping

## Slide 54
InP HBTs: 1.07 THz @200nm, ?? @ 130nm
?
Rode et al., IEEE TED, Aug. 2015